Supplementary Material

Fast and simple microwave synthesis of TiO2/Au nanoparticles for gas-phase photocatalytic hydrogen generation

Anna May-Masnou1*, Lluís Soler2*, Miquel Torras1, Pol Sallés1, Jordi Llorca2 and Anna Roig1

* Correspondence: Dr. Anna May-Mansou: amay@icmab.es, Dr. Lluís Soler: lluis.soler.turu@upc.edu

Supplementary Figure 1. Electron diffraction patterns of sample A (A) as-synthesized, (B) calcined at 450 °C and (C) calcined at 600 °C, and sample B (D) as-synthesized, (E) calcined at 450 °C and (F) calcined at 600 °C.

Supplementary Table 1. Size of the Au and TiO2 NPs for samples A and B at different calcination temperatures.

|  | Sample A |  | Sample B |  |
| --- | --- | --- | --- | --- |
| Thermal treatment | Size (nm) | n[a] | Size (nm) | n |
| Au |  |  |  |  |
| Not calcined | 52 ± 19 | 819 | 8 ± 2 | 651 |
| 400C | 57 ± 18 | 152 | N/A[b] | N/A |
| 450C | 49 ± 16 | 73 | 13 ± 4 | 157 |
| 550C | 51 ± 21 | 30 | 12 ± 3 | 46 |
| 600C | 59 ± 21 | 64 | 28 ± 9 | 73 |
| TiO2 |  |  |  |  |
| Not calcined | 9 ± 2 | 972 | 9 ± 2 | 521 |
| 400C | 8 ± 2 | 118 | N/A | N/A |
| 450C | 10 ± 2 | 202 | 9 ± 2 | 403 |
| 550C | 12 ± 4 | 167 | 10 ± 5 | 194 |
| 600C | 13 ± 4 | 59 | 17 ± 5 | 100 |

[a] n = number of NPs counted. [b] N/A = not available

Supplementary Figure 2. Size variation with temperature of the thermal treatment for Au and TiO2 NPs.

Supplementary Figure 3. Size variation with temperature of the thermal treatment for (A) Sample A and (B) Sample B. Histograms for particle size of samples calcined at 450 °C: (C) Au NPs in Sample A, (D) Au NPs in Sample B, (E) TiO2 NP in Sample A, (F) TiO2 NPs in Sample B.

Supplementary Figure 4. TGA of samples A and B as synthesized, and of PVP in air. The mass lost during the analysis of samples A and B corresponds to the PVP, whereas the mass remaining corresponds to Au and TiO2 and a fraction of not decomposed PVP. The dry residue for sample A is around 80 wt%, whereas for sample B is 77 wt%. This involves that of the total PVP present in the initial sample (31 wt% in sample A), only 64.5 wt% was decomposed. In sample B, the values are similar, 60.5 wt% of the PVP was decomposed. PVP decomposition started at 350 °C and finished around 470 °C. On the other hand, when pure PVP is treated under the same conditions, only a small residue around 5 wt% remains, so almost 95 wt% of the sample is decomposed, and the starting decomposition temperature is somewhat higher, around 375 °C. The TiO2/Au NPs act as catalyst for PVP decomposition, leading to a different decomposition behavior than for pure PVP. This is in agreement with the results obtained when studying the decomposition of Pt-PVP (PVP of 40 k) (Du et al., 2006). We considered these values to determine the mass of PVP that remains at each temperature, to express correctly the photocatalytic results as a function of metallic Au or TiO2 mass.

Supplementary Figure 5. Infrared spectra of (A) pure PVP, PVP-covered TiO2 NPs, sample A (with PVP), and sample A calcined at 450 °C, and (B) pure PVP, PVP-covered TiO2 NPs, sample B (with PVP), and sample B calcined at 450 °C. Compared with the spectra of pure PVP, the characteristic resonance peaks in the spectra of PVP-covered TiO2 NP, and of samples A and B around 3400 cm-1 and 2850 cm-1, and 1421 cm-1, assigned to -OH and -CH2 stretching, and -CH2 bending, respectively, present no relevant changes. The stretching vibration peak of C=O, originally at 1658 cm-1 in pure PVP, showed a slight red-shift to 1647 cm-1 for TiO2 NP, and to 1646 cm-1 for sample A and 1645 cm-1 for sample B, revealing the formation of a weak donor-acceptor type interaction by transfer of nonbonding electrons of the O-atom of PVP molecules to the NPs surface. The stretching vibration peaks of C-N, originally at 1072 cm-1, were strengthened and shifted to 1087 cm-1 in the TiO2/Au nanostructures (samples A and B) although the peak at 1285 cm-1 did not change. The IR spectra of the calcined samples at 450 °C proved that almost all the PVP was removed, since only a small peak on 1630 cm-1, corresponding to the C=O stretch, was present, but there was no presence of any other peaks, except from a small –OH around 3400 cm-1, indicating the hydration of the NPs.

Supplementary Figure 6. (A,B,C) TEM images of purified sample A*. (D) TEM image of 1st supernatant after centrifuging sample A. (E) TEM image of the 4th and last supernatant after centrifuging sample A.

Supplementary Figure 7. Chemical distribution of samples A and B, and purified A (A*) and B (B*). Percentages are in wt%.

Supplementary Figure 8. Samples used for the catalytic experiments.

Supplementary Figure 9. UV-Vis spectra between 350-800 nm wavelength of (A) sample A and (B) sample B as-synthesized, and purified (A*, B*) and of TiO2 before adding the gold precursor, (C) of the supernatants obtained from the purification of sample A, (D) of sample A as-synthesized (A), purified after 2 centrifugations, and purified after 4 centrifugations (A*). (E) Images of sample A as-synthesized, of the 4 supernatants, and of the final purified sample (A*).

Apparent Quantum Efficiency (AQE): The AQE was calculated following the equation AQE=2nH2np·100, where nH2 is the number of molecules of H2 generated and np the number of incident photons reaching the catalyst (Yu et al., 2013). The number of incident photons can be calculated by np=ETEp, where ET is the total energy reaching the catalyst and Ep is the energy of a photon. ET can be calculated by ET=PSt, where P (W·m-2) is the power density of the incident monochromatic light, S (m2) is the irradiation area and t (s) is the duration of the incident light exposure. Ep can be calculated by Ep=hc, where h is the Planck’s constant, c the speed of light and  (m) is the wavelength of the incident monochromatic light. The number of hydrogen molecules can be calculated as nH2=nNA, where n are H2 moles evolved during the time of light exposure (t), and NA is the Avogadro constant.

In our experimental conditions, the wavelength of the incident light was  = 365 nm, the power density of the incident light at the paper surface was P = 81.7 mW·cm-2 and the irradiation area was S = 2.54 cm2

References

Du, Y.K., Yang, P., Mou, Z.G., Hua, N.P., and Jiang, L. (2006). Thermal decomposition behaviors of PVP coated on platinum nanoparticles. Journal of Applied Polymer Science 99(1), 23-26. doi: 10.1002/app.21886.

Yu, Y.G., Chen, G., Hao, L.X., Zhou, Y.S., Wang, Y., Pei, J., et al. (2013). Doping La into the depletion layer of the Cd(0.6)Zn(0.4)S photocatalyst for efficient H(2) evolution. Chem Commun (Camb) 49(86), 10142-10144. doi: 10.1039/c3cc45568h.