# Supporting information

Tin Nanoparticles Encapsulated Carbon Nanoboxes as High-performance Anode for Lithium-Ion Batteries

Ziming Yang a, #, Hong-Hui Wub, #, Zhiming Zheng a, Yong Cheng a, Pei Li a, Qiaobao Zhang a, *, Ming-Sheng Wang a,*

a Department of Materials Science and Engineering, College of Materials, and Pen-Tung Sah

Institute of Micro-Nano Science and Technology, Xiamen University, Xiamen, Fujian 361005,

China.

b Department of Chemistry, University of Nebraska-Lincoln, NE 68588 Lincoln, United States

# CORRESPONDING AUTHOR

# Qiaobao Zhang, E-mail: zhangqiaobao@xmu.edu.cn

# Ming-Sheng Wang, E-mail: mswang@xmu.edu.cn

# These authors contributed equally to this work

The XRD pattern of Sn NPs is exhibited in Figure S1, the peak of which could be indexed to the Sn Phase (JCPDS No: 04-0673). As shown in Figure S2, the Precursor ZnSnO3 is Transformed into irregular Sn NPs(Sn nanoparticles) after heated at 600 °C for 5 h with a rate of 2 °C min-1 under H2 (5%)/Ar (95%) atmosphere.

Figure S1. XRD pattern of Sn NPs

Figure S2. SEM images of Sn NP samples.

The elemental mapping of ZnSnO3 is shown in Figure S3 and the energy dispersive spectrometer of ZnSnO3 is shown in Figure S4. The peak of Cu is from the copper substrate.

Figure S3. STEM image and its corresponding elemental mapping of ZnSnO3.

Figure S4. EDX of ZnSnO3.

As shown in Figure S6 and S7, it is obvious that the initial reversible discharge capacity of Sn@C is 806.5 mAh g-1 at 0.2 A g-1 and then the capacity gradually increases to 1032.2 mAh g-1 after 500 cycles. However, the Sn NPs shows an initial reversible discharge capacity of 923.3 mAh g-1 under the same conditions and then the capacity gradually decreases to 71.4 mAh g-1 after 100 cycles.

Figure S5. GCD curve of Sn NPs at 0.8 A g-1

Figure S6. (a) cycle performance at 0.2 A g-1, (b) the corresponding GCD curve of Sn@C at 0.2 A g-1

Figure S7. (a) cycle performance at 0.2 A g-1, (b) its corresponding GCD curve of SnNPs at 0.2 A g-1.

| Table S1 Comparison of electrochemical properties of Sn/C composites for LIBs |  |  |  |  |
| --- | --- | --- | --- | --- |
| Sample | Current density (mA g-1) | Cycle numbers | Capacity (mAh g-1) | Reference |
| Sn NP on CNTs | 3000 | 1000 | 537 | 7 |
| Pitaya-like Sn@C | 200 | 170 | 910 | 8 |
| Sn NP/Carbon | 200 | 200 | 865 | 9 |
| Core-shell Sn seeds | 400 | 600 | 870 | 10 |
| Yolk-shell Sn@C | 200 | 150 | 901 | 11 |
| Sn@C microsphere | 1000 | 500 | 537 | 12 |
| Yolk-shell Sn@C | 200 | 500 | 810 | 13 |
| Eggette-like Sn@C | 2000 | 800 | 550 | 14 |
| Sn@C nanoshpere | 200 | 800 | 430 | 15 |
| Sn NP/carbon sphere | 200 | 100 | 550 | 16 |
| Core-shell Sn@C | 75 | 100 | 566 | 17 |
| Sponge-like Sn@C | 200 | 300 | 1300 | 19 |
| Sn@C | 200 800 | 500 500 | 1030 670 | This work |