Supplementary Material

Chitosan Grafted with β-Cyclodextrin: Synthesis, Characterization, Antimicrobial Activity, and Role as Absorbefacient and Solubilizer

Wen-Ya Ding1,2,3+, Si-Di Zheng1,2+, Yue Qin1,2, Fei Yu1,2, Jing-Wen Bai4, Wen-Qiang Cui1,2, Tao Yu1,2, Xing-Ru Chen1,2, Bello-Onaghise God'spower1,2, Yan-Hua Li1,2*

1College of Veterinary Medicine, Northeast Agricultural University, Harbin, Heilongjiang 150030

2Heilongjiang Key Laboratory for Animal Disease Control and Pharmaceutical Development, Harbin, China

3Northeastern Science Inspection Station, China Ministry of Agriculture Key Laboratory of Animal Pathogen Biology, Northeast Agricultural University, Harbin, Heilongjiang 150030, China

4College of Science, Northeast Agricultural University, Harbin, China

*Correspondence to: Professor Yanhua Li, College of Veterinary Medicine, Northeast Agricultural University, 600 Changjiang Road, Xiangfang, Harbin, Heilongjiang 150030, P.R. China

Tel：+86 451 55191881

E-mail: liyanhua1970@163.com (Y.-H.Li).

†These authors have contributed equally to this study and share first authorship.

The characterization of the chemical structures of CS and β-CD

Figure 2A showed the 1H NMR spectrum of the β-CD. The proton signals at δ 4.9 ppm and the multiplet proton signals at δ 3.9–3.4 ppm, which were due to the H1 proton and H2–H6 protons, respectively (Gonil et al., 2011). According to Ben’s report (Ben Mihoub et al., 2018), the protons were further assigned as follows: The multiplet protons at δ=3.9–3.7 ppm were assigned to the H3, H5 and H6 protons. The multiplet protons at δ=3.6–3.4 ppm were assigned to the H2, H4 protons. The 1H NMR of CS is shown in Figure 2B. 1H NMR (DCl) δ=3.025 (H2) (Zhu et al., 2006). Due to the similar chemical environments and chemical shift of H3, H4, H5 and H6, the peaks covered each other. It has been reported that the H3 and H4 chemical shift of glucosamine are before H5 and H6 (Cui et al., 2017). Thus δ=3.764 ppm and 3.597 ppm resulted from the H3, H4 proton and H5, H6, respectively. The H1 chemical shift of chitosan is usually 4.4 to 5.0 and overlaps with solvent peak (And and Rinaudo, 2001).

The FT-IR of CS (Figure 2E) showed a broad -OH stretch spectrum at 3438.5 cm−1 and the C-H chain stretch within the 2990 and 2850 cm−1 range. The free primary amino group at C2 position was represented by the other major absorption within the 1220 and 1020 cm−1 region. The –C–O stretch of primary alcoholic group was observed at peak 1382.8 cm−1.

The standard curve of hydrolysis of β-CD

Fig. S1. The standard curve of hydrolysis of β-CD.

Linearity

The calibration curve prepared by plotting the absorbance versus concentration of sulfadiazine and sulfamonomethoxine from 4 to 8 μg/mL, the concentration of sulfamethoxazole were 4 μg/mL, 6 μg/mL, 8 μg/mL, 10 μg/mL and 12 μg/mL, respectively, consisting of five concentrations analyzed in solutions of authentic standards; the calibration curve was the average of five authentic standard curves. The maximum absorption wavelength of sulfadiazine, sulfamonomethoxine and sulfamethoxazole were 254nm, 262nm and 257nm, which was determined after scanning the wavelength range of the UV–Vis spectrophotometer. The linear equation of sulfadiazine, sulfamonomethoxine and sulfamethoxazole were ,  and  and the linear correlation coefficient (R2) were 0.9995, 0.9987 and 0.9981, respectively.

Precision

The precision was determined by analyzing sulfadiazine, sulfamonomethoxine and sulfamethoxazole of known concentrations at three levels. The solutions of sulfadiazine and sulfamonomethoxine were prepared in 0.1mol/LNaOH and sulfamethoxazole was prepared in absolute ethyl alcohol with concentrations at the minimum, intermediate and maximum linearity points defined in the linearity test. The solutions and samples were analyzed in triplicate on different days, and the concentrations were recalculated each time using the calibration curve obtained for the UV–Vis method. Table. S1 presents the precision results used to validate the UV–Vis method presented as an average of triplicate measurements on different days ± the standard deviation and the associated %RSD. The precision evaluation of the proposed method yielded RSDs below 2% at all evaluated levels and the precision was satisfactory.

Table. S1. Precision evaluation for the analytical validation of the UV–Vis method for sulfadiazine, sulfamonomethoxine and sulfamethoxazole quantification (n = 3).

| Sample | Add Concentration（μg/mL） | Day | Intra-day precision | Inter-day precision |
| --- | --- | --- | --- | --- |
|  |  |  | Measured concentration（μg/mL） | RSD（%） | Measured concentration（μg/mL） | RSD（%） |
| sulfadiazine | 4 | 1st day | 3.85±0.04 | 0.91 | 3.91±0.05 | 1.36 |
|  |  | 2nd day | 3.95±0.02 | 0.42 |  |  |
|  |  | 3rd day | 3.95±0.02 | 0.56 |  |  |
|  | 6 | 1st day | 5.91±0.02 | 0.28 | 5.86±0.09 | 1.53 |
|  |  | 2nd day | 5.75±0.07 | 1.19 |  |  |
|  |  | 3rd day | 5.92±0.03 | 0.47 |  |  |
|  | 8 | 1st day | 7.99±0.04 | 0.55 | 7.96±0.06 | 0.71 |
|  |  | 2nd day | 7.90±0.02 | 0.28 |  |  |
|  |  | 3rd day | 8.01±0.02 | 0.28 |  |  |
| sulfamonomethoxine | 4 | 1st day | 4.01±0.04 | 0.90 | 4.13±0.06 | 1.56 |
|  |  | 2nd day | 3.98±0.03 | 0.78 |  |  |
|  |  | 3rd day | 3.94±0.06 | 1.64 |  |  |
|  | 6 | 1st day | 5.95±0.03 | 0.43 | 5.99±0.05 | 0.88 |
|  |  | 2nd day | 5.97±0.02 | 0.41 |  |  |
|  |  | 3rd day | 6.04±0.05 | 0.81 |  |  |
|  | 8 | 1st day | 11.58±0.08 | 0.65 | 7.91±0.08 | 0.95 |
|  |  | 2nd day | 11.90±0.07 | 0.56 |  |  |
|  |  | 3rd day | 11.71±0.07 | 0.57 |  |  |
| sulfamethoxazole | 4 | 1st day | 3.83±0.06 | 1.55 | 4.13±0.06 | 1.56 |
|  |  | 2nd day | 3.90±0.03 | 0.64 |  |  |
|  |  | 3rd day | 3.94±0.05 | 1.23 |  |  |
|  | 8 | 1st day | 7.96±0.03 | 0.43 | 8.48±0.12 | 1.39 |
|  |  | 2nd day | 8.11±0.05 | 0.62 |  |  |
|  |  | 3rd day | 7.90±0.13 | 1.62 |  |  |
|  | 12 | 1st day | 11.58±0.08 | 0.65 | 12.44±0.15 | 1.21 |
|  |  | 2nd day | 11.90±0.07 | 0.56 |  |  |
|  |  | 3rd day | 11.71±0.07 | 0.57 |  |  |

Stability

The stability were determined that three replicates of the quality control samples at 6μg/mL of sulfadiazine, sulfamonomethoxine and 8μg/mL of sulfamethoxazole were processed and analyzed according to requirements, respectively. The stability test was performed by keeping the samples for 0h, 1h, 2h, 4h, 6h, 8h, 24h at room temperature before analysis. The stability of sulfadiazine, sulfamonomethoxine and sulfamethoxazole are shown in the Table. S2. This result indicated that sulfadiazine, sulfamonomethoxine and sulfamethoxazole were stable at room temperature for 24h.

Table. S2. The stability evaluation of the UV–Vis method for sulfadiazine, sulfamonomethoxine and sulfamethoxazole at room temperature (n = 3).

| Sample | Add Concentration（μg/mL） | Measured concentration（μg/mL） | RSD (%) |
| --- | --- | --- | --- |
|  |  | 0h | 1h | 2h | 4h | 6h | 8h | 24h |  |
| sulfadiazine | 6 | 5.98± 0.078 | 6.04± 0.058 | 6.13± 0.013 | 5.89± 0.047 | 5.95± 0.055 | 6.14± 0.043 | 6.02± 0.054 | 1.95 |
| sulfamonomethoxine | 6 | 6.09± 0.060 | 6.09± 0.026 | 5.93± 0.021 | 6.12± 0.018 | 5.88± 0.018 | 6.12± 0.046 | 6.13± 0.015 | 1.8 |
| sulfamethoxazole | 8 | 7.97± 0.046 | 7.88± 0.052 | 8.17± 0.019 | 8.19± 0.023 | 8.23± 0.033 | 8.06± 0.161 | 8.05± 0.047 | 1.95 |

Recovery

The percentage recovery was determined by analyzing sulfadiazine and sulfamonomethoxine at concentrations of 6μg/mL, sulfamethoxazole of 8μg/mL respectively. Since no certified reference material existed, 6.061µg/mL sulfadiazine and sulfamonomethoxine were added to 6μg/mL, 8.108µg/mL sulfamethoxazole were added to 8μg/mL. The solutions and samples were analyzed in triplicate, and the concentrations were recalculated each time using the calibration curve obtained for the UV–Vis method. From Table. S3, We obtained average recoveries above 98%, with RSDs below 2% at all levels investigated. These results showing that instrumental and reagent manufacturer variations did not influence the sulfadiazine, sulfamonomethoxine and sulfamethoxazole quantification.

Table. S3. Recovery evaluation for the analytical validation of the UV–Vis method for  sulfadiazine, sulfamonomethoxine and sulfamethoxazole quantification.

| Sample | Concentration（μg/mL） | Add Concentration（μg/mL） | Recovery rate mean (%) | RSD(%) |
| --- | --- | --- | --- | --- |
| sulfadiazine | 6 | 6.061 | 98.98±0.21 | 0.88 |
| sulfamonomethoxine | 6 | 6.061 | 99.5±0.67 | 0.64 |
| sulfamethoxazole | 8 | 8.108 | 99.2±0.23 | 0.76 |

Reference

And, R.A., and Rinaudo, M. (2001). Chitosan Derivatives Bearing Pendant Cyclodextrin Cavities: Synthesis and Inclusion Performance. Macromolecules 34(11), 3574-3580.

Ben Mihoub, A., Saidat, B., Bal, Y., Frochot, C., Vanderesse, R., and Acherar, S. (2018). Development of new ionic gelation strategy: Towards the preparation of new monodisperse and stable hyaluronic acid/beta-cyclodextrin-grafted chitosan nanoparticles as drug delivery carriers for doxorubicin. Frontiers of Materials Science 12(1), 83-94. doi: 10.1007/s11706-018-0407-2.

Cui, G.H., Zhao, D.H., Lv, P., Gao, Z.G., Chen, S.Y., Qiu, N.N., et al. (2017). Synthesis and characterization of Eu(III)-based coordination complexes of modified D-glucosamine and poly(N-isopropylacrylamide). Optical Materials 72, 115-121. doi: 10.1016/j.optmat.2017.05.051.

Gonil, P., Sajomsang, W., Ruktanonchai, U.R., Pimpha, N., Sramala, I., Nuchuchua, O., et al. (2011). Novel quaternized chitosan containing β-cyclodextrin moiety: Synthesis, characterization and antimicrobial activity. Carbohydrate Polymers 83(2), 905-913.

Zhu, A., Chen, T., Yuan, L., Wu, H., and Lu, P. (2006). Synthesis and characterization of N-succinyl-chitosan and its self-assembly of nanospheres. Carbohydrate Polymers 66(2), 274-279. doi: 10.1016/j.carbpol.2006.03.014.