Supplementary Material

Breathable and Wearable MXene-Decorated Air-Laid Paper with Outstanding Folding Endurance and Electromagnetic Interference Shielding Performances

Chang Maa, Tong Liua, Wei Xina, Guo-Qiang Xia,b, Ming-Guo Maa*

aEngineering Research Center of Forestry Biomass Materials and Bioenergy, Beijing Key Laboratory of Lignocellulosic Chemistry, College of Materials Science and Technology, Beijing Forestry University, Beijing 100083, PR China；

bKey Laboratory for Green Processing of Chemical Engineering of Xinjiang Bingtuan, School of Chemistry and Chemical Engineering, Shihezi University, Shihezi 832003, Xinjiang, PR China.

Figure S1. Digital image of MAX phase and the Tyndall effect of MXene nanosheets aqueous suspension after etching.

Figure S2. The SEM image of MAX phase.

Figure S3. The TEM image of MXene nanosheets.

Figure S4. XRD patterns of MAX (Ti3AlC2) phase and MXene nanosheets.

Figure S5. Oxidation stability of MP-20 after a period of time.

Figure S6. SEM images of (a) the original MP-20; (b) MP-20 after folding; (c) MP-20 after treating by artifical sweat; (d) MP-20 after 5 weeks.

Table S1. Comparison of the EMI shielding performance of the MXene/air-laid paper composite and the other materials.

| Sample | Type | Materials | Thickness(mm) | SSE/t(dB cm2g-1) | Reference |
| --- | --- | --- | --- | --- | --- |
| 1 | Metal based Carbon | copper | 3.1 | 32.3 | (Shui et al, 1997) |
| 2 |  | Ni fiber/PES | 2.85 | 108.7 | (Shui et al, 1997) |
| 3 |  | SS | 4 | 27.5 | (Li et al, 1994) |
| 4 |  | CuNi/CNT | 1.5 | 1580 | (Ji et al., 2014) |
| 5 |  | Ag NW/PI | 0.5 | 2416 | (Ma et al., 2015) |
| 6 |  | SS/PP | 3.1 | 241.9 | (Ameli et al., 2014) |
| 7 |  | Graphene/PS | 2.5 | 692 | (Yan et al., 2015) |
| 8 | based MXene based | Graphene/PEDOT | 0.8 | 841 | (Dalal et al., 2016) |
| 9 |  | Graphene/Fe3O4 | 0.3 | 1033 | (Song et al., 2015) |
| 10 |  | MWCNT/PC | 2.1 | 163 | (Pande et al., 2014) |
| 11 |  | SWCNT/PS | 1.2 | 275 | (Yang et al., 2005) |
| 12 |  | CB/ABS | 1.1 | 190 | (Al-Saleh et al., 2013) |
| 13 |  | CB/EPDM | 2 | 15.1 | (Chakrabarti, 2000) |
| 14 |  | Carbon foam | 2 | 1250 | (Moglie et al., 2012) |
| 15 |  | Ti3C2Tx/CNFs | 0.047 | 2647 | (Cao et al., 2018) |
| 16 |  | MXene/air-laid paper | 0.119 | 1931.5 | This work |
|  |  |  | 0.117 | 2001.4 |  |
|  |  |  | 0.116 | 1941.9 |  |

Note:

PES- polyethersulfone

CNT- carbon nanotube

SS- stainless steel

NW- nanowire

PI- polyimide

PP- polypropylene

PS- polystyrene

PEDOT- poly(3,4-ethylenedioxythiophene)

MWCNT- multi-wall carbon nanotube

SWCNT- single-wall carbon nanotube

PC- polycarbonate

CB- carbon black

ABS- acrylonitrile butadiene styrene copolymers

EPDM- ethylene propylene diene monomer

CNFs- cellulose nanofibers

Table S2. The mechanical properties of the MXene/air-laid paper composite sheets in different dip-coating cycle numbers.

| Sample | Tensile strength (Mpa) | Tensile strain (%) | Young’s modulus (MPa) | Folding endurance |
| --- | --- | --- | --- | --- |
| Original Air-laid paper | 17.34±3.55 | 64.72±6.49 | 103.70±30.49 | 99750 |
| MP-3 | 20.36±2.34 | 53.08±3.87 | 144.69±47.41 | 96539 |
| MP-5 | 23.26±2.07 | 56.61±4.84 | 183.57±58.84 | 98301 |
| MP-10 | 16.97±3.81 | 54.54±2.61 | 152.51±75.45 | 99572 |
| MP-20 | 16.73±1.45 | 55.69±4.64 | 94.70±28.73 | 97564 |

References

Al-Saleh, M.H., Saadeh, W.H.,Sundararaj, U. (2013). EMI shielding effectiveness of carbon based nanostructured polymeric materials: A comparative study. Carbon 60, 146-156. doi:10.1016/j.carbon.2013.04.008

Ameli, A., Nofar, M., Wang, S.,Park, C.B. (2014). Lightweight Polypropylene/Stainless-Steel Fiber Composite Foams with Low Percolation for Efficient Electromagnetic Interference Shielding. ACS Applied Materials & Interfaces 6, 11091-11100. doi:10.1021/am500445g

Cao, W., Chen, F., Zhu, Y., Zhang, Y., Jiang, Y.,Ma, M., et al. (2018). Binary Strengthening and Toughening of MXene/Cellulose Nanofiber Composite Paper with Nacre-Inspired Structure and Superior Electromagnetic Interference Shielding Properties. ACS Nano 12, 4583-4593. doi:10.1021/acsnano.8b00997

Dalal, J., Gupta, A., Lather, S., Singh, K., Dhawan, S.K.,Ohlan, A. (2016). Poly (3, 4-ethylene dioxythiophene) laminated reduced graphene oxide composites for effective electromagnetic interference shielding. Journal of Alloys and Compounds 682, 52-60. doi:10.1016/j.jallcom.2016.04.276

Ji, K., Zhao, H., Zhang, J., Chen, J.,Dai, Z. (2014). Fabrication and electromagnetic interference shielding performance of open-cell foam of a Cu–Ni alloy integrated with CNTs. Applied Surface Science 311, 351-356. doi:10.1016/j.apsusc.2014.05.067

Lin Li,Chung, D.D.L. (1994). Electrical and mechanical properties of electrically conductive polyethersulfone composites. Composites 25, 215-224. doi:10.1016/0010-4361(94)90019-1

Ma, J., Wang, K.,Zhan, M. (2015). A comparative study of structure and electromagnetic interference shielding performance for silver nanostructure hybrid polyimide foams. RSC Advances 5, 65283-65296. doi:10.1039/c5ra09507g

Moglie, F., Micheli, D., Laurenzi, S., Marchetti, M.,Mariani Primiani, V. (2012). Electromagnetic shielding performance of carbon foams. Carbon 50, 1972-1980. doi:10.1016/j.carbon.2011.12.053

Pande, S., Chaudhary, A., Patel, D., Singh, B.P.,Mathur, R.B. (2014). Mechanical and electrical properties of multiwall carbon nanotube/polycarbonate composites for electrostatic discharge and electromagnetic interference shielding applications. RSC Advances 4, 13839. doi:10.1039/c3ra47387b

Premamoy Ghosh,Chakrabarti, A. (2000). Conducting carbon black filled EPDM vulcanizates: assessment of dependence of physical and mechanical properties and conducting character on variation of filler loading. EUROPEAN POLYMER JOURNAL, 1043-1054. doi:10.1016/S0014-3057(99)00157-3

Shui, X.,Chung, D.D.L. (1997). Nickel filament polymer-matrix composites with low surface impedance and high electromagnetic interference shielding effectiveness. Journal of Electronic Materials 26, 928-934. doi:10.1007/s11664-997-0276-4

Song, W., Guan, X., Fan, L., Cao, W., Wang, C.,Zhao, Q., et al. (2015). Magnetic and conductive graphene papers toward thin layers of effective electromagnetic shielding. Journal of Materials Chemistry A 3, 2097-2107. doi:10.1039/C4TA05939E

Yan, D., Pang, H., Li, B., Vajtai, R., Xu, L.,Ren, P., et al. (2015). Structured Reduced Graphene Oxide/Polymer Composites for Ultra-Efficient Electromagnetic Interference Shielding. Advanced Functional Materials 25, 559-566. doi:10.1002/adfm.201403809

Yang, Y., Gupta, M.C., Dudley, K.L.,Lawrence, R.W. (2005). Novel Carbon Nanotube−Polystyrene Foam Composites for Electromagnetic Interference Shielding. Nano Letters 5, 2131-2134. doi:10.1021/nl051375r