Table S3. Radial width of xylem and cell wall thickness in stems of control and PmCesA2 transgenic poplar plants. Data are the mean value ± SD of three biological replicates. * denotes significance at p < 0.05.

| Samples | Radial width of xylem (μm) | Wall thickness (μm) |
| --- | --- | --- |
| WT | 1835 ± 34.1 | 1.20 |
| L 15 | 3651 ± 78.04* | 3.01* |
| L 7 | 2584 ± 57.76* | 2.68* |
| L 12 | 2872 ± 61.58* | 2.86* |