Supporting Information

for

Enhanced Circularly Polarized Luminescence Activity in Chiral Platinum(II) Complexes with Bis- or Tri-phenylphosphine Ligands

Qian-Ying Yang 1, Hua-Hong Zhang 1, Xue-Ling Han 1, Shi-Dao Weng 1, Yuan Chen 1, Jia-Li Wu 1, Li-Zhi Han 1, Xiao-Peng Zhang 1*, Zai-Feng Shi 1

1 Key Laboratory of Water Pollution Treatment & Resource Reuse of Hainan Province, College of Chemistry and Chemical Engineering, Hainan Normal University, Haikou 571158, China

* Correspondence: 
Xiao-Peng Zhang
zxp_inorganic@126.com

Materials and methods, crystal structures, spectroscopic properties and TD-DFT calculation results

Table of Contents

1. Materials and Methods .......................................................................................... 2

2. Crystal structures ................................................................................................... 4

3. Spectroscopic properties ........................................................................................ 6

4. TD-DFT calculation results ..................................................................................10

5. References ............................................................................................................ 13

# 1.  Materials and Methods

1.1  General Methods

All reagents were purchased from commercial suppliers and used as received. Mass spectra were acquired on an LCQ Fleet ESI Mass Spectrometer. The NMR spectra were obtained on Bruker DRX-400 spectrometer. Coupling constants are given in hertz. UV-vis spectra were measured on a UV-3600 spectrophotometer. Elemental analysis was performed on a Perkin-Elmer 240C analyzer. Photoluminescence (PL) spectra were measured by Hitachi F-4600 PL spectrophotometer (λex = 420 nm). The circular dichroism (CD) spectra in CH2Cl2 solution were recorded on a Jasco J-810 spectropolarimeter at a scan rate of 100 nm·min−1 and 1 nm resolution at room temperature (using 10 mm quartz cell for concentration of 510-5 mol·L-1, bandwidth = 1 nm, response = 1 sec, accumulations = 3). The CPL spectra in CH2Cl2 solution were recorded a Jasco CP-300 spectrofluoropolarimeter at a scan rate of 100 nm·min−1 and 1 nm resolution at room temperature (using 10 mm quartz cell for concentration of 10-3 mol·L-1, Ex wavelength = 330 nm, D.I.T. = 2 sec, Ex slit width = 4000 μm, Em slit width = 4000 μm, Detector:	PM-539, Detector S/N: B0005PM539, Lock-in amp.: X mode, HT volt = 670-720V, Accessory: RSC-502, Accessory S/N: A0005RSC502, accumulations = 10).

1.2  Single Crystal X-ray Structure Determination

Single-crystal X-ray diffraction measurements were carried out on a Bruker SMART APEX CCD based on diffractometer operating at 153 K. Intensities were collected with graphite monochromatized Mo Kα radiation (λ = 0.71073 Å) operating at 50 kV and 30 mA, using ω/2θ scan mode. The data reduction was made with the Bruker SAINT package.[1] Absorption corrections were performed using the SADABS program.[2] The structures were solved by direct methods and refined on F2 by full-matrix least-squares using SHELXL-97 with anisotropic displacement parameters for all non-hydrogen atoms in all two structures. Hydrogen atoms bonded to the carbon atoms were placed in calculated positions and refined as riding mode, with C−H = 0.93 Å (methane) or 0.96 Å (methyl) and Uiso(H) = 1.2Ueq (Cmethane) or Uiso(H) = 1.5Ueq (Cmethyl). The water hydrogen atoms were located in the difference Fourier maps and refined with an O-H distance restraint [0.85(1) Å] and Uiso(H) = 1.5 Ueq(O). All computations were carried out using the SHELXTL-97 program package.[3] CCDC 1984372-1984374 contain the supplementary crystallographic data for this paper. These data can be obtained free of charge from The Cambridge Crystallographic Data Centre via www.ccdc.cam.ac.uk/data_request/cif.

1.3  Calculation Methods

Crystal structures (−)-3-OTf, (−)-4 and (−)-7 were used as the starting geometry, and optimization was performed by the Gaussian09 program.[4] The starting structures of (−)-5 and (−)-6 are based on the crystal structure (−)-3-OTf that adding one carbon atom on the bridging ligands. The CAM-B3LYP functional was used, SVP basis set for C, H, N, and P, and MWB60 pseudopotential basis set for Pt, and the conductor-like polarizable continuum solvent model (CPCM).[5] TD-DFT simulations was performed with same functional and basis sets. The calculated CD spectrum was drawn by using the software SpecDis,[6] in which the sigma/eV was set at 0.2.

# 2.  Crystal structures

Table S1 Bond lengths of complexes (−)-3-OTf, (−)-4 and (−)-7 determined by X-ray single crystal diffraction.

| Bond Lengths | (−)-3-OTf | (−)-4 | (−)-7 |
| --- | --- | --- | --- |
| Pt1−C1 | 2.016(5) | 1.972(7) | 2.043(7) |
| Pt2−C2 | 2.007(6) | 1.994(9) | 2.025(7) |
| Pt1−N1 | 1.985(5) | 1.998(5) | 2.0175(18) |
| Pt1−N2 | 2.119(5) | 2.167(6) | 2.135(6) |
| Pt2−N3 | 1.984(6) | 1.973(6) | 2.014(6) |
| Pt2−N4 | 2.108(4) | 2.104(7) | 2.143(6) |
| Pt1−P1 | 2.2478(17) | 2.2503(18) | 2.2445(19) |
| Pt2−P2 | 2.245(2) | 2.241(2) | 2.2522(19) |
| Pt3−C3 |  | 2.019(8) |  |
| Pt4−C4 |  | 2.006(8) |  |
| Pt3−P3 |  | 2.259(2) |  |
| Pt4−P4 |  | 2.2351(19) |  |
| Pt3−N5 |  | 1.998(6) |  |
| Pt3−N6 |  | 2.146(6) |  |
| Pt4−N7 |  | 2.016(6) |  |
| Pt4−N8 |  | 2.118(6) |  |

Table S2 Bond angles around Pt(II) nucleus of complexes (−)-3-OTf, (−)-4, (−)-7 and reported (−)-(C^N^N)PtCl, (−)-(C^N^N)PtPPV, (−)-(C^N^N)PtDmpi.

| Bond Angles | (−)-3-OTf | (−)-4 | (−)-7 | (C^N^N)PtCl | (C^N^N)Pt PPV- Form-Y | (C^N^N)PtPPV- Form-O | (C^N^N)Pt Dmpi- Form-Y | (C^N^N)PtDmpi- Form-R |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| C1−Pt1−N2 | 158.8(2) | 159.4(3) | 158.9(3) . | 162.2(4) | 160.75(16) | 160.88(15) | 160.1(10) | 162.3(4) |
| N1−Pt1−P1 (Cl1, C2) | 176.10(16) | 171.79(18) | 174.51(10) | 178.0(2) | 176.7(2) | 178.23(15) | 177.6(12) | 175.3(4) |
| C2−Pt2−N4 | 158.7(3) | 157.9(3) | 159.0(3) | 162.4(5) |  |  | 161.2(5) |  |
| N3−Pt2−P2 (Cl2, C4) | 173.60(15) | 168.75(17) | 174.6(2) | 178.2(3) |  |  | 178.2(13) |  |
| C3−Pt3−N6 |  | 157.3(3) |  |  |  |  |  |  |
| N5−Pt3−P3 |  | 173.57(18) |  |  |  |  |  |  |
| C4−Pt4−N8 |  | 158.3(3) |  |  |  |  |  |  |
| N7−Pt4−P4 |  | 169.63(19) |  |  |  |  |  |  |

Table S3 Torsion angles between the benzene plane and lateral pyridine plane of C^N^N ligands in complexes (−)-3-OTf, (−)-4 and (−)-7.

| Torsion angles | (−)-3-OTf | (−)-4 | (−)-7 |
| --- | --- | --- | --- |
| benzene(1) − pyridine(1) | 7.281(153) | 5.191(216) | 8.160(289) |
| benzene(2) − pyridine(2) | 8.224(183) | 11.209(250) | 1.333(312) |
| benzene(3) − pyridine(3) |  | 14.514(265) |  |
| benzene(4) − pyridine(4) |  | 9.412(232) |  |

Figure S1 Intermolecluar PtPt contacts of complex (−)-3-OTf, (−)-4 and (−)-7. H atoms and anions are omitted for clarity.

2.  Spectroscopic properties

Figure S2 Absorption spectra and emission spectrum of (−)-4 in CH2Cl2 (5×10-5 mol·L-1) at T = 298 K, λex = 420 nm (top); CD spectra in CH2Cl2 (510-5 mol·L-1) at T = 298 K (middle); CPL spectra in CH2Cl2 (10-3 mol·L-1) at T = 298 K (middle); gabs and glum factors (bottom).

Figure S3 Absorption spectra and emission spectrum of (−)-4 in CH2Cl2 (5×10-5 mol·L-1) at T = 298 K, λex = 420 nm (top); CD spectra in CH2Cl2 (510-5 mol·L-1) at T = 298 K (middle); CPL spectra in CH2Cl2 (10-3 mol·L-1) at T = 298 K (middle); gabs and glum factors (bottom).

Figure S4 Absorption spectra and emission spectrum of (−)-4 in CH2Cl2 (5×10-5 mol·L-1) at T = 298 K, λex = 420 nm (top); CD spectra in CH2Cl2 (510-5 mol·L-1) at T = 298 K (middle); CPL spectra in CH2Cl2 (10-3 mol·L-1) at T = 298 K (middle); gabs and glum factors (bottom).

Figure S5 Emission spectra of (−)-3, (−)-4, (−)-5, (−)-6 and (−)-7 at 298 (solid line) and 77 K (dash line) (λex = 420 nm).

2.  TD-DFT calculation results

Figure S6 The optimized configurations of all the chiral dinuclear and mononuclear Pt(II) complexes.

Figure S7 Simulated rotatory strength (green), and CD spectrum (red) of complex (−)-3 in dichloromethane solution in comparison with its experimental one (black).

Figure S8 Simulated rotatory strength (green), and CD spectrum (red) of complex (−)-4 in dichloromethane solution in comparison with its experimental one (black).

Figure S9 Simulated rotatory strength (green), and CD spectrum (red) of complex (−)-5 in dichloromethane solution in comparison with its experimental one (black).

Figure S10 Simulated rotatory strength (green), and CD spectrum (red) of complex (−)-6 in dichloromethane solution in comparison with its experimental one (black).

Figure S11 Simulated rotatory strength (green), and CD spectrum (red) of complex (−)-7 in dichloromethane solution in comparison with its experimental one (black).

5.  References

- [1] SAINT-Plus, version 6.02, Bruker Analytical X-ray System: Madison, WI, 1999.

- [2] G. M. Sheldrick, SADABS, an empirical absorption correction program, Bruker Analytical X-ray Systems: Madison, WI, 1996.

- [3] G. M. Sheldrick, Acta Cryst., 2008, A64, 112.

- [4] Frisch, M. J. T., G. W.; Schlegel, H. B.; Scuseria, G. E.; Robb, M. A.; Cheeseman, J. R.; Scalmani, G.; Barone, V.; Mennucci, B.; Petersson, G. A.; Nakatsuji, H.; Caricato, M.; Li, X.; Hratchian, H. P.; Izmaylov, A. F.; Bloino, J.; Zheng, G.; Sonnenberg, J. L.; Hada, M.; Ehara, M.; Toyota, K.; Fukuda, R.; Hasegawa, J.; Ishida, M.; Nakajima, T.; Honda, Y.; Kitao, O.; Nakai, H.; Vreven, T.; Montgomery, J. A., Jr.; Peralta, J. E.; Ogliaro, F.; Bearpark, M.; Heyd, J. J.; Brothers, E.; Kudin, K. N.; Staroverov, V. N.; Kobayashi, R.; Normand, J.; Raghavachari, K.; Rendell, A.; Burant, J. C.; Iyengar, S. S.; Tomasi, J.; Cossi, M.; Rega, N.; Millam, J. M.; Klene, M.; Knox, J. E.; Cross, J. B.; Bakken, V.; Adamo, C.; Jaramillo, J.; Gomperts, R.; Stratmann, R. E.; Yazyev, O.; Austin, A. J.; Cammi, R.; Pomelli, C.; Ochterski, J. W.; Martin, R. L.; Morokuma, K.; Zakrzewski, V. G.; Voth, G. A.; Salvador, P.; Dannenberg, J. J.; Dapprich, S.; Daniels, A. D.; Farkas, O.; Foresman, J. B.; Ortiz, J. V.; Cioslowski, J.; Fox, D. J. Gaussian 09, Gaussian, Inc.: Wallingford CT, 2013.

- [5] Klamt, A., J. Phys. Chem., 1995, 99, 2224-2235.

[6] Bruhn, T., Schaumlöffel, A., Hemberger, Y., SpecDis version 1.63, University of Wuerzburg, Germany, 2015.