Supporting Information

Rational design of the platinahelicene enantiomers for deep-red circularly polarized organic light-emitting diodes

Zhi-Ping Yan, Xu-Feng Luo, Kang Liao, You-Xuan Zheng*, Jing-Lin Zuo*

State Key Laboratory of Coordination Chemistry, Jiangsu Key Laboratory of Advanced Organic Materials, School of Chemistry and Chemical Engineering, Nanjing University, Nanjing 210093, P. R. China

* Correspondence: 
Corresponding Author
yxzheng@nju.edu.cn, zuojl@nju.edu.cn

Content

S1. High resolution mass spectrum of (RAC)-Pt

S2. Chiral HPLC analysis of (RAC)-Pt enantiomers

S3. NMR spectra for P-Pt and M-Pt

S4. X-ray crystallographic data

S5. Photophysical data for (RAC)-Pt, P-Pt and M-Pt

S6 Electrochemical data

S7. Thermal stability

S8. Device performance characterization of P-SD, M-SD, P-DD and M-DD

S1. High resolution mass spectrum of (RAC)-Pt

Figure S1. High resolution mass spectrum of (RAC)-Pt.

S2. Chiral HPLC analysis of (RAC)-Pt enantiomers

Figure S2. Chiral HPLC profile of (RAC)-Pt.

<Column Performance Report>

| Peak# | Ret. Time | Area | Area% | T.Plate# | Tailing F. | Resolution |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 3.812 | 2470126 | 49.684 | 6377 | 1.268 | -- |
| 2 | 5.976 | 2501570 | 50.316 | 7745 | 1.262 | 9.360 |

Figure S3. Chiral HPLC profile of P-Pt.

<Column Performance Report>

| Peak# | Ret. Time | Area | Area% | T.Plate# | Tailing F. | Resolution |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 3.726 | 4732240 | 99.892 | 6151 | 1.268 | -- |
| 2 | 6.058 | 5118 | 0.108 | 7182 | 1.977 | 9.802 |

Figure S4. Chiral HPLC profile of M-Pt.

<Column Performance Report>

| Peak# | Ret. Time | Area | Area% | T.Plate# | Tailing F. | Resolution |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 3.776 | 4019 | 0.110 | 7134 | 1.021 | -- |
| 2 | 5.827 | 3639025 | 99.890 | 7363 | 1.314 | 9.108 |

S3. NMR spectra for P-Pt and M-Pt

Figure S5. 1H NMR spectrum of P-Pt.

Figure S6. 13C NMR spectrum of P-Pt.

Figure S7. 1H NMR spectrum of M-Pt.

Figure S8. 13C NMR spectrum of M-Pt.

S4. X-ray crystallographic data

Table S1. Crystal data and structure refinement for P-Pt and M-Pt.

| Identification code | P-Pt | M-Pt |
| --- | --- | --- |
| CCDC | 1844425 | 1844426 |
| Empirical formula | C35H31F4NO2Pt | C35H31F4NO2Pt |
| Formula weight | 768.7 | 768.7 |
| Temperature/K | 296(2) | 296(2) |
| Crystal system | Orthorhombic | Orthorhombic |
| Space group | P212121 | P212121 |
| a/Å | 10.3804(11) | 10.3788(9) |
| b/Å | 12.2412(13) | 12.2284(10) |
| c/Å | 24.215(2) | 24.193(2) |
| α/° | 90 | 90 |
| β/° | 90 | 90 |
| γ/° | 90 | 90 |
| Volume/Å3 | 3077.0(6) | 3070.5(4) |
| Z | 4 | 4 |
| ρcalcg/cm3 | 1.659 | 1.663 |
| μ/mm-1 | 4.616 | 4.626 |
| F(000) | 1512 | 1512 |
| Radiation | MoKα (λ = 0.71073) | MoKα (λ = 0.71073) |
| 2Θ range for data collection/° | 3.36 to 54.46 | 3.36 to 55.02 |
| Index ranges | -13 ≤ h ≤ 13, -15 ≤ k ≤ 9, -30 ≤ l ≤ 31 | -13 ≤ h ≤ 13, -15 ≤ k ≤ 11, -31 ≤ l ≤ 31 |
| Reflections collected | 20528 | 20924 |
| Independent reflections | 6852 [Rint = 0.0369, Rsigma = 0.0545] | 7050 [Rint = 0.0436, Rsigma = 0.0608] |
| Data/restraints/parameters | 6852/890/394 | 7050/896/394 |
| Goodness-of-fit on F2 | 1.117 | 0.996 |
| Final R indexes [I>=2σ (I)] | R1 = 0.0313, wR2 = 0.0618 | R1 = 0.0337, wR2 = 0.0753 |
| Final R indexes [all data] | R1 = 0.0377, wR2 = 0.0633 | R1 = 0.0425, wR2 = 0.0786 |
| Largest diff. peak/hole / e Å-3 | 0.70/-0.64 | 0.76/-0.81 |
| Flack parameter | 0.007(8) | 0.009(9) |

R1a = ||Fo|  |Fc||/Fo|. wR2b = [w(Fo2  Fc2)2/w(Fo2)]1/2

S5. Photophysical data for (RAC)-Pt, P-Pt and M-Pt

Figure S9. Transient decay curve of (RAC)-Pt in CH2Cl2 (5×10-5 M).

Figure S10. gPL vs. wavelength curves of P-Pt and M-Pt in (a) CH2Cl2 (5×10-5 M) and (b) doped film (5 wt% in 26DCzPPy).

Figure S11. CD spectra of P-Pt and M-Pt before (dash) and after sublimation (solid).

Table S2. Photophysical data for (RAC)-Pt.

| Complex Configuration |  | λPL nm | λECD nm (mdeg) | gPL /10-3 |  | τ μs | Ф |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  |  |  | Solution | film |  |  |
| (RAC)-Pt | P | 650 | 253(-277),287(-15),314(162),361(95),446(7) | -5.9 | -3.8 | 4.6 | 0.04 |
|  | M |  | 253(296),287(16),314(-172),361(-100),446(-7) | 6.0 | 4.2 |  |  |

S6 Electrochemical data

Table S3. Electrochemical data of P-Pt and M-Pt.

| Complex | Eox,onset (Pt)a V | Ered,onset (Pt)b V | Eox,onset (Fe)c V | Eg,optd eV | EHOMO/ELUMOe eV |
| --- | --- | --- | --- | --- | --- |
| P-Pt | 0.83 | -1.17 | 0.05 | 2.34 | -5.58/ -3.24 |
| M-Pt | 0.83 | -1.19 | 0.05 | 2.34 | -5.58/ -3.24 |
| a: The onset of oxidation of Pt(II) complexes; b: The onset of reduction curves of Pt(II) complexes; c: The onset of oxidation curves of Ferrocene; d: Optical gap (= 1240/λonset); e: EHOMO = -[Eox - E(Fc/Fc+) + 4.8] eV, ELUMO = EHOMO + Eg. |  |  |  |  |  |

S7. Thermal stability

Figure S12. TGA curve of (RAC)-Pt recorded under nitrogen at a heating rate of 10 oC min-1.

S8. Device performance characterization of P-SD, M-SD, P-DD and M-DD

Figure S13. (a) Device configurations of CP-OLEDs; (b) Chemical structures of adopted materials.

S12. Device performance characterization of P-SD, M-SD, P-DD and M-DD

Figure S14. Characteristics of devices P-SD, M-SD, P-DD and M-DD: (a) Current density-luminance-voltage (J-L-V) curves; (b) Current efficiency-current density curves (inset: normalized EL spectra at 8 V).