Supporting Information

to

Hierarchical Porous Graphene-Iron Carbide Hybrid Derived from Functionalized Graphene-Based Metal-Organic Gel as Efficient Electrochemical Dopamine Sensor

Eleni C. Vermisoglou1†, Petr Jakubec1†, Ondřej Malina1, Vojtěch Kupka1, Andreas Schneemann2,3, Roland A. Fischer2, Radek Zbořil1, Kolleboyina Jayaramulu1,2,4 and Michal Otyepka1*

1 Faculty of Science, Regional Centre of Advanced Technologies and Materials, Palacký University Olomouc, Olomouc, Czechia, 2 Inorganic and Metal-Organic Chemistry, Department of Chemistry and Catalysis Research Centre, Technical University of Munich, Garching, Germany, 3 Lehrstuhl für Anorganische Chemie I, Technische Universität Dresden, Bergstr, Germany, 4 Department of Chemistry, Indian Institute of Technology Jammu, Jammu & Kashmir, India

Corresponding author: michal.otyepka@upol.cz

† Equally contributed this work.

SCHEME S1. Schematic Illustration of synthesis metal-organic gel by using iron (III) and 5-aminoisopthalate.

Scheme S2. Tube inversion method: A gel prepared in a vial/tube was inversed in order to see if there is a flow of the solvent or if the solvent is immobilized (gel). This is a very common test that is used widely in literature related to gel preparation (Huynh et al., 2017, Nguyen et al., 2014).

Huynh, C. T., Zheng, Z., Nguyen, M. K., McMillan, A., Tonga, G. Y., Rotello, V. M., et al. (2017). Cytocompatible Catalyst-Free Photodegradable Hydrogels for Light- Mediated RNA Release To Induce hMSC Osteogenesis. ACS Biomater. Sci. Eng. 3, 2011-2023. https://pubs.acs.org/doi/10.1021/acsbiomaterials.6b00796

Nguyen M. K., Jeon, O., Krebs, M. D., Schapira, D., Alsberg E. (2014). Sustained localized presentation of RNA interfering molecules from in situ forming hydrogels to guide stem cell osteogenic differentiation. Biomaterials 35, 6278-6286. http://dx.doi.org/10.1016/j.biomaterials.2014.04.048

FTIR spectroscopy

In Figures S1c, S1d  the absence of the characteristic band at 1680-1730 cm-1, related to the protonated carboxylate group, indicates complete deprotonation of the ligand Niso in MOG, MOG@IG powder samples and implies metal coordinating carboxylate groups (Zhang et al., 2007).  The absorption peaks at 3066-3339 cm-1 were assigned to N-H stretching vibrations and moisture (Wang et al., 2017). The N-H absorptions of Niso overlap with the much broader O-H absorption of water molecules in MOG@IG sample due to hydrogen bonding between amino groups and water molecules. The absorption band range 712-772 cm-1 can be assigned to δ(O-C-O) vibrations of the ligand Niso (Zhou et al., 2016).

FIGURE S1. FTIR spectra of: (a) GrF, (b) IG, (c) MOG powder, (d) MOG@IG powder, (e) MGH-400, (f) MGH-600, and (g) MGH-800.

Wang, Y., Zhang, L. J., Zhang, R., Jin, Y., Wang, Y., Xing, et al. (2017). Porous Metal-Organic Frameworks with 5‑Aminoisophthalic Acid as Platforms for Functional Applications about High Photodegradation Efficiency of Phenol. Cryst. Growth Des. 17, 6531-6540. https://doi.org/10.1021/acs.cgd.7b01190.

Zhang, K. L., Qiao, N., Gao, H. Y., Zhou, F., and Zhang, M. (2007). Self assembly of two novel three-dimensional supramolecular networks with blue photoluminescence. Polyhedron 26, 2461-2469. https://doi.org/10.1016/j.poly.2006.12.047.

Zhou, Y. Y., Geng, B., Zhang, Z. W., and Bo, Q. B. (2016). Synthesis, structures and photoluminescence of three d10 5-aminonicotinate and 5-aminoisophthalate coordination polymers with bilayer structures. Inorg. Chim. Acta 444, 150-158. https://doi.org/10.1016/j.ica.2016.02.001.

XPS spectroscopy

X-ray photoelectron spectroscopy (XPS) was employed in order to determine the elemental composition and chemical state of atoms in MOG@IG powder composite. The XPS survey spectra is presented in Figure S2a and reveals for the elements C, N, O, Fe, F the following atomic concentrations (at. %): 58.4, 7.5, 26.0, 7.0 and 1.1, respectively. The C1s XPS spectrum of MOG@IG compared to that of IG (Figure S2b) clearly indicates the presence of the ligand functional groups. The atomic percentage of carboxylate groups -C=O has increased by a factor of ~2.4 and C-N (or C-N/C-O) groups were doubled. The content of C-F group remains in similar level, while the sp2 C in C=C and sp3 C in C-C are reduced since the content of graphene in the composite is lower (complete details presented in Table S1). High resolution Fe 2p XPS spectrum (Figure S2c) exhibits two peaks centered at 725.4 and 711.5 eV and their satellites at 732.4 eV and 715.6 eV ascribed to Fe 2p1/2  and Fe 2p3/2 of Fe3+, correspondingly. These satellite peaks constitute the fingerprint of Fe3+ electronic structures and imply the absence of Fe2+. The peak separation is ~13.9 eV and can be attributed to α-Fe2O3 nodes in the MOG framework (Yu et al., 2019) equal to the peak separation for MIL-100 (Fe) (Lv et al., 2015), evidencing similar structure in accordance to XRD results. In Figure S2d the high resolution O 1s XPS spectrum is depicted where the peaks at 530.1, 531.8 and 533.3 eV are assigned to the Fe-O, O=C and O-C bonds in MOG@IG in accordance with literature (Yang et al., 2016).

FIGURE S2. (a) XPS survey spectrum of MOG@IG powder; (b) High-resolution C 1s spectra of IG (bottom) and MOG@IG (top), (c) high resolution Fe 2p and (d) high resolution O1s spectra of MOG@IG.

Lv, H., Zhao, H., Cao, T., Qian, L., Wang, Y., and Zhao, G. (2015). Efficient degradation of high concentration azo-dye wastewater by heterogeneous Fenton process with iron-based metal-organic framework. J. Molec. Catal. A Chem. 400, 81-89. https://doi.org/10.1016/j.molcata.2015.02.007.

Yang, Q., Zhao, Q., Ren, S. S., Lu, Q., Guo, X., and Chen, Z. (2016). Fabrication of core-shell Fe3O4@MIL-100(Fe) magnetic microspheres for the removal of Cr(VI) in aqueous solution. J. Solid State Chem. 244, 25-30, https://doi.org/10.1016/j.jssc.2016.09.010.

Yu, D., Wu, M., Hu, Q., Wang, L., Lv, C., and Zhang, L. (2019). Iron-based metal-organic frameworks as novel platforms for catalytic ozonation of organic pollutant: Efficiency and mechanism, J. Hazard. Mater. 367, 456-464. https://doi.org/10.1016/j.jhazmat.2018.12.108.

TABLE S1. Atomic percentage (at. %) of various groups in IG and MOG@IG composite obtained from deconvolution of high resolution C1s XPS spectra.

| Samples | C-C (sp2) ~284.7 eV | C-C (sp3) ~285.8 eV | C-N ~286.6 eV | O=C-O ~288.5 eV | C-F ~290.1 eV |
| --- | --- | --- | --- | --- | --- |
| IG | 62.5 | 17.8 | 7.5 | 9.6 | 2.6 |
| MOG@IG | 49.5 | 10.3 | 14.5 | 23.4 | 2.3 |

Raman spectroscopy

The signals at ~790 cm-1, ~1000 cm-1 and ~1595 cm-1 in MOG (Figure S3, bottom) can be attributed to the –COO- deformation mode and C-C aromatic ring vibrations, respectively. Additionally, the asymmetric and symmetric stretching vibrations of carboxylates correspond to the Raman bands at ~1416 and ~1538 cm-1. C-H vibration modes appear in the range 2800-3000 cm-1. In the Raman spectrum of MOG@IG (Figure S3, top) the graphene characteristics prevail as it is documented by the D and G peaks.

FIGURE S3. Raman spectra of MOG powder (bottom) and MOG@IG powder (top).

FIGURE S4. Mӧssbauer spectrum of MOG@IG powder.

TABLE S2. Values of the Mössbauer hyperfine parameters derived from the fitting procedure, where T is the temperature of the measurement, δ is the isomer shift, ΔEQ is the quadrupole splitting, Bhf is the hyperfine magnetic field and RA is relative spectra area of each component. *The average quadrupole splitting derived from the distribution of the quadrupole splitting parameter (see inset in Figure S10b). T-sites and O-sites denote the tetrahedral and octahedral sites in the Fe3O4 crystal structure.

| Sample | T (K) | Component | δ ± 0.01 (mm/s) | ΔEQ ± 0.01 (mm/s) | Bhf ± 0.3 (T) | RA ± 1 (%) | Assignment |
| --- | --- | --- | --- | --- | --- | --- | --- |
| MOG@IG MGH-400 MGH-600 MGH-800 | 300 300 | Doublet Doublet Sextet 1 Sextet 2 Sextet 3 Sextet 1 Sextet 2 Sextet 3 Sextet 4 Doublet Sextet 1 Sextet 2 | 0.42 0.82 0.66 0.28 0.19 0.00 0.20 0.60 0.35 0.35 0.00 0.19 | 0.81 0.91* 0.00 0.00 0.00 0.00 0.00 0.00 0.00 0.89 0.00 0.00 | -- -- 46.0 49.1 20.7 33.0 20.6 46.0 49.5 -- 33.0 20.6 | 100 11 52 33 4 78 18 2 2 5 50 45 | Fe3+ ions Fe3+ ions Magnetite – O-sites Magnetite – T-sites Fe3C nZVI Fe3C Magnetite – O-sites Magnetite – T-sites Fe3+ ions nZVI Fe3C |

FIGURE S5. (a) SEM and (b) TEM micrographs of MOG@IG (before solvent removal); (c) TEM image of MOG@IG powder (after solvent removal).

FIGURE S6. XRD patterns of: (a) MGH-400, (b) MGH-600 and (c) MGH-800 samples (Co-Kα radiation source, 40 kV, 30 mA, λ= 0.1789 nm).

FIGURE S7. Raman spectra of: (a) MGH-400 and (b) MGH-800 samples (inset: 2D peak).

FIGURE S8. SEM images of: (a) MGH-400, (b) MGH-600 and (c) MGH-800 samples.

FIGURE S9. TEM images of: (a) MGH-400, (b) MGH-600 and (c) MGH-800 samples.

FIGURE S10. Mӧssbauer spectra of: (a) MOG@IG powder, (b) MGH-400, (c) MGH-600 and (d) MGH-800 samples measured at 300 K.

FIGURE S11.  N2 adsorption/desorption isotherms obtained at -196 °C for (a) MOG@IG powder, (b) MGH-400, (c) MGH-600 and (d) MGH-800 samples and the corresponding BET Surface Areas.

FIGURE S12. Pore size distributions derived using the DFT kernel for slit pores from the desorption branch of the isotherm for (a) MOG@IG powder, (b) MGH-400, (c) MGH-600 and (d) MGH-800 samples.

FIGURE S13. CV response of the bare glassy carbon electrode (GCE) and GCE modified with different samples (MOG@IG, MGH-400, MGH-600 and MGH-800) in the presence of PBS buffer (pH 7.0) containing both dopamine (cDA = 2.5 mmol L–1) and ascorbic acid (cAA = 2.5 mmol L–1).

TABLE S3. Comparison table of Raman peak intensity ratios (ID/IG), BET specific surface areas and iron derivatives present in pyrolyzed samples MGH-400, MGH-600 and MGH-800.

| Sample | ID/IG | BET (m2/g) | Fe-derivatives |
| --- | --- | --- | --- |
| MGH-400 | 1.4 | 84 | Fe3C, FeO, Fe3O4 |
| MGH-600 | 0.9 | 218 | Fe, Fe3C, Fe3O4 |
| MGH-800 | 0.7 | 179 | Fe, Fe3C, Fe3O4, Fe2O3 |

FIGURE S14. Stability test of MGH-600 sample. CV response of fresh MGH-600 sample (green line) and 15 months old MGH-600 sample (orange line) recorded at glassy carbon electrodes (GCEs) in the presence of PBS buffer (pH 7.0) containing both dopamine (cDA = 2.5 mmol L–1) and ascorbic acid (cAA = 2.5 mmol L–1).

FIGURE S15. Microscopically investigated stability of MGH-600 sample. (a, b) TEM images of MGH-600 obtained after 15 months, (c) HRTEM image of an iron containing nanoparticle of the MGH-600 sample obtained after this term.

TABLE S4. List of various MOF-derived/Iron based hybrid nanocomposites (recent literature) which are compared in terms of performance in DA sensing.

| Material | Method | Linear Range (μM) | LOD (μM) | Ref. | Year |
| --- | --- | --- | --- | --- | --- |
| OFMs | Electrochemical | 0.2-115 | 0.03 | 1 | 2018 |
| Fe3O4@Cu silicate sea urchins | Electrochemical | 100-200 | 3.2 | 2 | 2018 |
| ZIF-8-AB-CS/GCE | Electrochemical | 0.1-10 | 0.004 | 3 | 2018 |
| Fe2O3 NPs/GRS | Electrochemical | 0.01-195.18 | 0.004 | 4 | 2018 |
| ACC-α-Fe2O3 | Electrochemical | 0.074-113 | 0.050 | 5 | 2018 |
| α-Fe2O3@erGO | Electrochemical | 0.25-100 | 0.024 | 6 | 2018 |
| γ-Fe2O3 nanobelts/GCE | Electrochemical | 0.6-15 | 0.6 | 7 | 2018 |
| GO-ZIF67 | Electrochemical | 0.2-80 | 0.050 | 8 | 2018 |
| Nafion/PANI/ZIF-8 | Electrochemical | 0.1-100 | 0.012 | 9 | 2018 |
| PPy/ZIF-67-MIPs/Nafion | Electrochemical | 0.08-100 100-500 | 0.0308 | 10 | 2018 |
| Eu-MOF | Fluorescent | 0-60 | 0.015 | 11 | 2019 |
| HKUST-1/GCE | Electrochemical | 12.5-175 | 0.11 | 12 | 2019 |
| Fe3O4@Au@tyrosinase | Fluorescent | 10-100 | 1 | 13 | 2019 |
| Fe3O4/GO/PG | Electrochemical | 0.30-30 | 0.18 | 14 | 2019 |
| Fe2O3/GO | Electrochemical | 0.3-30 | 0.18 | 15 | 2019 |
| sulfo-MIL-101-GPE | Electrochemical | 0.07-100 | 0.043 | 16 | 2019 |
| NH2-MIL-125 PA-MIL 125 | Fluorescent Fluorescent | 0.05-0.5 0.05-0.5 | 0.01 0.005 | 17 | 2019 |
| Fe3O4-40 | Electrochemical | 0.002-0.6 | 0.008 | 18 | 2019 |
| 3D-rGO/Fe3O4/HP-β-CD/GCE | Electrochemical | 0.02-25 | 0.0067 | 19 | 2019 |
| MOF/ERGO | Electrochemical | 0.2-300 | 0.013 | 20 | 2019 |
| Au@Fe3O4/GCE | Electrochemical | 0-0.8 | 0.0027 | 21 | 2019 |
| Ni-ZIF-8/N S-CNTs/CS/GCE | Electrochemical | 8-500 | 0.93 | 22 | 2020 |
| MGH-600 | Electrochemical | 0.5-5 10-50 | 0.44 | This work | 2020 |

[1] Chen, X., Liu, Q., Liu, M., Zhang, X., Lin, S., Chen, Y.,  et al. (2018). Protein-templated Fe2O3 microspheres for highly sensitive amperometric detection of dopamine. Microchim.  Acta 185, 340. https://doi.org/10.1007/s00604-018-2876-5.

[2] Das, A. K., Kuchi, R., Van, P. C., Sohn, Y., and Jeong, J. R. (2018). Development of an Fe3O4@Cu silicate based sensing platform for the electrochemical sensing of dopamine. RSC Adv. 8,31037-31047. https://doi.org/10.1039/C8RA05885G.

[3] Jin, Y. F., Ge,C. Y., Li, X. B., Zhang, M.,  Xu, G. R.,  and Li, D. H. (2018). A sensitive electrochemical sensor based on ZIF-8–acetylene black–chitosan nanocomposites for rutin detection.  RSC Adv. 8, 32740-32746.  https://doi.org/10.1039/C8RA06452K.

[4] Kokulnathan, T., Anthuvan, A. J., Chen, S. M., Chinnuswamy, V., and Kadirvelu, K. (2018). Trace level electrochemical determination of the neurotransmitter dopamine in biological samples based on iron oxide nanoparticle decorated graphene sheets. Inorg. Chem. Front. 5, 705-718. https://doi.org/10.1039/C7QI00716G.

[5] Mahesh, K. P. O., Shown, I., Chen, L. C., Chen, K. H., and Tai, Y. (2018). Flexible sensor for dopamine detection fabricated by the direct growth of α-Fe2O3 nanoparticles on carbon cloth. Appl. Surf. Sci. 427, 387-395.  https://doi.org/10.1016/j.apsusc.2017.08.168.

[6] Mathew, G., Dey, P.,  Das, R., Chowdhury, S. D., Das, M. P., Veluswamy, P., et al. (2018). Direct electrochemical reduction of hematite decorated graphene oxide (α- Fe2O3@erGO) nanocomposite for selective detection of Parkinson's disease biomarker, Biosens. Bioelectron. 115, 53-60. https://doi.org/10.1016/j.bios.2018.05.024.

[7] Sundar, S., Venkatachalam, G., and Kwon, S. J. (2018). Sol-Gel Mediated Greener Synthesis of  γ-Fe2O3 Nanostructures for the Selective and Sensitive Determination of Uric Acid and Dopamine. Catalysts 8, 512; doi:10.3390/catal8110512.

[8] Tang, J., Jiang, S., Liu, Y., Zheng, S., Bai, L., Guo, J., et al. (2018). Electrochemical determination of dopamine and uric acid using a glassy carbon electrode modified with a composite consisting of a Co(II)-based metalorganic framework (ZIF-67) and graphene oxide. Microchim. Acta 185, 486. https://doi.org/10.1007/s00604-018-3025-x

[9] Yuan, Y., Xia, J., Zhang, F., Wang, Z., and Liu, Q. (2018). Nafion/polyaniline/Zeolitic Imidazolate Framework-8 nanocomposite sensor for the electrochemical determination of dopamine. J. Electroanal. Chem. 824, 147-152. https://doi.org/10.1016/j.jelechem.2018.07.048.

[10] Zhang, W., Duan, D., Liu, S., Zhang, Y., Leng, L., Li, X., et al. (2018). Metal-organic framework-based molecularly imprinted polymer as a high sensitive and selective hybrid for the determination of dopamine in injections and human serum samples. Biosens. Bioelectron. 118, 129-136. https://doi.org/10.1016/j.bios.2018.07.047.

[11] Du, Q., Wu, P., Dramou, P., Chen, R., and He, H. (2019). One-step fabrication of a boric acid-functionalized lanthanide metal–organic framework as a ratiometric fluorescence sensor for the selective recognition of dopamine. New J. Chem. 43, 1291-1298. https://doi.org/10.1039/C8NJ05318A.

[12] Sofi, F. A., Bhat, M. A., and Majid, K. (2019). Cu2+-BTC based metal–organic framework: a redox accessible and redox stable MOF for selective and sensitive electrochemical sensing of acetaminophen and dopamine. New J. Chem. 43, 3119-3127.  https://doi.org/10.1039/C8NJ06224B.

[13] Arkan, E., Karami, C., and Rafipur, R. (2019). Immobilization of tyrosinase on Fe3O4@Au core-shell nanoparticles as bio‑probe for detection of dopamine, phenol and catechol. J. Biol. Inorg. Chem. 24, 961-969.  https://doi.org/10.1007/s00775-019-01691-0.

[14] Cai, L., Hou, B., Shang, Y., Xu, L., Zhou, B., Jiang, X., et al. (2019). Synthesis of Fe3O4/graphene oxide/pristine graphene ternary composite and fabrication electrochemical sensor to detect dopamine and hydrogen peroxide. Chem. Phys. Lett. 736, 736, 136797. https://doi.org/10.1016/j.cplett.2019.136797.

[15] Cai, Z., Ye, Y., Wan, X., Liu, J., Yang, S., Xia, Y., et al. Morphology–Dependent Electrochemical Sensing Properties of Iron Oxide–Graphene Oxide Nanohybrids for Dopamine and Uric Acid. Nanomaterials 9, 835. https://doi.org/10.3390/nano9060835.

[16] Gao, L. L., Sun, W. J., Yin, X. M., Bu, R., and Gao,W. Q. (2019). Graphite paste electrodes modified with a sulfo-functionalized metal-organic framework (type MIL-101) for voltammetric sensing of dopamine, Microchim. Acta 186, 762.  https://doi.org/10.1007/s00604-019-3943-2.

[17] George, P., and  Chowdhury, P. (2019). NH2-MIL-125(Ti) and its emeraldine functionalized derivative as a chemical sensor for effective detection of dopamine. Micropor. Mesopor. Mater. 288, 109591. https://doi.org/10.1016/j.micromeso.2019.109591.

[18] Huang, Y., Zhang, Y., Liu, D., Li, M., Yu, Y., Yang, W., et al. (2019). Facile synthesis of highly ordered mesoporous Fe3O4 with ultrasensitive detection of dopamine. Talanta 201, 511-518. https://doi.org/10.1016/j.talanta.2019.01.099.

[19] Liang, W., Rong, Y., Fan, L., Zhang, C., Dong, W.,  Li, J.,  et al. (2019). Simultaneous electrochemical sensing of serotonin, dopamine and ascorbic acid by using a nanocomposite prepared from reduced graphene oxide, Fe3O4 and hydroxypropyl-β-cyclodextrin. Microchim. Acta 186, 751. https://doi.org/10.1007/s00604-019-3861-3.

[20] Ma, B., Guo, H., Wang, M., Li, L., Jia, X., Chen, H., et al. (2019). Electrocatalysis of Cu-MOF/Graphene Composite and its Sensing Application for Electrochemical Simultaneous Determination of Dopamine and Paracetamol. Electroanalysis 31, 1002-1008. https://doi.org/10.1002/elan.201800890.

[21] Thamilselvan, A., Manivel, P., Rajagopal, V., Nesakumar, N., and Suryanarayanan, V. (2019). Improved electrocatalytic activity of Au@Fe3O4 magnetic nanoparticles for sensitive dopamine detection, Colloids Surf. B 180, 1-8.  https://doi.org/10.1016/j.colsurfb.2019.04.034.

[22] Yao, W., Guo, H., Liu, H., Li, Q., Wu, N., Li, L., et al. (2020). Highly electrochemical performance of Ni-ZIF-8/ N S-CNTs/CS composite for simultaneous determination of dopamine, uric acid and L-tryptophan.  Microchem. J. 152, 104357. https://doi.org/10.1016/j.microc.2019.104357.

ABBREVIATIONS

OFMs: Olive-like Fe2O3 microspheres.

Fe3O4@Cu silicate sea urchins: sea urchin like Fe3O4@Cu silicate core–shell nanocomposites.

ZIF-8-AB-CS/GCE: Glassy carbon electrode (GCE) modified with zeolitic imidazolate framework-8 (ZIF-8) and acetylene black (AB) in the presence of chitosan (CS).

Fe2O3 NPs/GRS: Iron oxide nanoparticle-(Fe2O3 NP) capped graphene sheet (GRS) modified glassy carbon electrode (GCE).

ACC-α-Fe2O3: Porous α-Fe2O3 nanoparticles directly grown on acid treated carbon cloth (ACC) using a hydrothermal method.

α-Fe2O3@erGO: Magnetic hematite (α-Fe2O3) decorated electrochemically reduced graphene oxide (α-Fe2O3@erGO) nanocomposite.

γ-Fe2O3 nanobelts/GCE:  γ-Fe2O3 nanostructures modified glassy carbon electrode (GCE).

GO-ZIF67: Composite consisting of a Co(II)-based metalorganic framework (ZIF-67) and graphene oxide.

Nafion/PANI/ZIF-8: Nafion/polyaniline/Zeolitic Imidazolate Framework-8 nanocomposite fabricated on the surface of glassy carbon electrode (GCE).

PPy/ZIF-67-MIPs/Nafion/GCE: Molecular imprinting polymer (MIP) sensor fabricated based on polypyrrole (PPy)/ZIF-67/Nafion hybrid modified glassy carbon electrode (GCE).

Eu-MOF: Boric acid-modified lanthanide metal–organic framework.

HKUST-1/GCE: HKUST-1 modified glassy carbon electrode (GCE).

Fe3O4@Au@tyrosinase: Bio-probe based on the immobilized tyrosinase on Fe3O4@Au core-shell nanoparticles.

Fe3O4/GO/PG: Fe3O4/graphene oxide (GO)/pristine graphene (PG) ternary composite.

Fe2O3/GO: Discal Fe2O3 NPs coupled with graphene oxide (GO) nanosheets casted on glassy carbon electrode (GCE).

sulfo-MIL-101-GPE: Sulfo-functionalized metal-organic framework (type MIL-101) modified graphite paste electrode (GPE).

NH2-MIL-125: NH2 functionalized MIL-125 (Ti) Metal Organic Framework (MOF).

PA-MIL 125: Emeraldine–NH2–MIL-125(Ti).

Fe3O4-40: Ordered mesoporous Fe3O4 with high surface area modified glassy carbon electrode.

3D-rGO/Fe3O4/HP-β-CD/GCE: Nanocomposite prepared from reduced graphene oxide, Fe3O4 and hydroxypropyl-β-cyclodextrin deposited on glassy carbon electrode (GCE).

MOF/ERGO: A nanocomposite of HKUST-1 (MOF) and electroreduction graphene oxide (ERGO) deposited on glassy carbon electrode (GCE).

Au@Fe3O4/GCE: Gold (Au) nanoparticles (NPs) systematically decorated with magnetic Fe3O4 nanocomposites deposited on glassy carbon electrode (GCE).

Ni-ZIF-8/N S-CNTs/CS/GCE: Ni-ZIF-8, N S-CNTs (carbon nanotubes), chitosan composite deposited on glassy carbon electrode (GCE).