Supplementary Figure 1: Molecular structures of (A) isoniazid (INH) (B) pyrazinamide (PZA), and (C) pentanedioic acid (GA)

Supplementary Table 1: Summary of the co-crystal screening for isoniazid (INH) and pyrazinamide (PZA) with pentanedioic acid (GA) as a co-former

| API | co-former | Ratios | Method | Solvent | Outcome |
| --- | --- | --- | --- | --- | --- |
| INH | GA | (1:1) | DG | none | INHGA (1:1) co-crystal |
|  |  | (2:1) | DG | none | INHGA (2:1) co-crystal |
| PZA | GA | (2:1) | DG | none | PGA (2:1) co-crystal |
|  |  | (2:1) | LAG | Ethanol 96% | PGA (2:1) co-crystal |

(NB: DR= dry grinding, LAG= liquid assisted grinding, and SE= solvent evaporation)

Supplementary Figure 2: HSM images of pentanedioic acid (GA), isoniazid (INH), the co-crystals INHGA (2:1), PGA (2:1) and pyrazinamide (PZA) recorded over 25-200 °C temperature range.

Supplementary Figure 3: Standard calibration curves for isoniazid (INH) and pyrazinamide (PZA) for INHGA (2:1), PGA (2:1) co-crystals.