Supplementary Material

# Supplementary Data

Supplementary Material should be uploaded separately on submission. Please include any supplementary data, figures and/or tables. All supplementary files are deposited to FigShare for permanent storage and receive a DOI.

Supplementary material is not typeset so please ensure that all information is clearly presented, the appropriate caption is included in the file and not in the manuscript, and that the style conforms to the rest of the article. To avoid discrepancies between the published article and the supplementary material, please do not add the title, author list, affiliations or correspondence in the supplementary files.

# Supplementary Figures and Tables

2.1 Supplementary Table S1. Biodegradation Certification Systems

1. Certifications based on industrial composting test

| Country | Certification |  | Label |
| --- | --- | --- | --- |
| European Union | Std. Name Assoc. | DIN EN 13432 OK Compost Industrial / Seedling TÜV AUSTRIA, DIN CERTCO |  |
|  | Std. Name Assoc. | AS 5810(2010), NF T 51800(2015), prEN 17427(2020) OK Compost Home / DIN-Geprüft Home Compostable TÜV AUSTRIA / DIN CERTCO |  |
| Germany | Std. Name Assoc. | DIN EN 13432 DIN-Geprüft DIN CERTCO |  |
| Italy | Std. Name Assoc. | EN 13432 Compostable CIC The Italian Composting and Biogas Association |  |
| United States | Std. Name Assoc. | ASTM 5338, ASTM 6400, ASTM 6868 BPI Certification Mark Biodegradable Products Institute |  |
| Australia | Std. Name Assoc. | AS 4736 Seedling Australasian Bioplastics Association, DIN CERTCO |  |
|  | Std. Name Assoc. | AS5810(2010) Home Compostable Australasian Bioplastics Association, DIN CERTCO |  |
| Korea | Std. Name Assoc. | KS M ISO 14855 Korea Eco-Label Korea Environmental Industry & Technology Institute |  |
| Japan | Std. Name Assoc. | JIS K 6950, JIS K 6951, JIS K 6953-1, JIS K 6955 GreenPla Japan Bioplastics Association (JPBA) |  |
| China | Std. Name Assoc. | GB/T 19276.1, GB/T 19276.2, GB/T 32106 GB/T 19277.1(2011) Biodegradable Plastic Logo China National Light Industry Council |  |

2. Certifications based on soil, marine, aquatic test

| Country | Certification |  | Label |
| --- | --- | --- | --- |
| Belgium | Std. Name Assoc. | TÜV AUSTRIA’s Own Standard OK Biodegradable Water, OK Biodegradable Soil, OK Biodegradable Marine TÜV AUSTRIA |  |
| Germany | Std. Name Assoc. | DIN EN 17033 DIN-Geprüft biodegradable in soil DIN CERTCO |  |

Supplementary Table S2. Biodegradation Study Results

1. PLA-based bioplastics

| Bioplastic | Environment | Condition |  | Indicator | Period (day) | Biodegradability (%) | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Temp. (℃) | etc |  |  |  |  |
| PLA | Composting | 58 |  | CO2 produced | 60 | 13 | H.K. Ahn et al., 2011 |
| PLA/Starch/Poultry feather (80/15/5) | Composting | 58 |  | CO2 produced | 60 | 53 | H.K. Ahn et al., 2011 |
| PLA | Composting | 58 | Humidity=90% | CO2 produced | 58 | 84 | G. Kale et al., 2007 |
| PLA | Composting | 65 | Nature, pH=8.5, humidity=63% | Weight loss | 30 | >90 | G. Kale et al., 2007 |
| PLA | Composting | 55 |  | CO2 produced | 28 | 70 | R.Y. Tabasi, A. Ajji., 2015 |
| PLA/PBAT (50/50) | Composting | 55 |  | CO2 produced | 28 | 43~45 | R.Y. Tabasi, A. Ajji., 2015 |
| PLA | Composting | 55 |  | Weight loss | 30 | 60 | M. Mihai et al., 2014 |
| PLA/Wood fiber (70/30) | Composting | 55 |  | Weight loss | 30 | 40 | M. Mihai et al., 2014 |
| PLA (with foaming agent; PS) | Composting | 58 | Humidity=55% | Weight loss | 90 | 63.6 | J. Sarasa et al., 2009 |
| PLA/corn (90/10) | Composting | 58 | Humidity=55% | Weight loss | 90 | 79.7 | J. Sarasa et al., 2009 |
| PLA | Composting | 58 | Humidity=55% | Weight loss | 28 | >90 | M.P. Arrieta et al., 2014 |
| plasticized PLA (with ATBC) | Composting | 58 | Humidity=55% | Weight loss | 28 | >90 | M.P. Arrieta et al., 2014 |
| plasticized PLA (with PEG) | Composting | 58 | Humidity=55% | Weight loss | 28 | >90 | M.P. Arrieta et al., 2014 |
| plasticized PLA/PHB (75/25, with ATBC) | Composting | 58 | Humidity=55% | Weight loss | 28 | >90 | M.P. Arrieta et al., 2014 |
| plasticized PLA/PHB (75/25, with PEG) | Composting | 58 | Humidity=55% | Weight loss | 35 | >90 | M.P. Arrieta et al., 2014 |
| PLA | Composting | 58 | Humidity=55% | Weight loss | 84 | 42.3 | M.P. Balaguer et al., 2016 |
| PLA | Composting | 58 | Humidity=55% | CO2 produced | 130 | >70 | M.P. Balaguer et al., 2016 |
| PLA + Clay1 | Composting | 58 | Humidity=55% | Weight loss | 84 | 41.6 | M.P. Balaguer et al., 2016 |
| PLA + Clay1 | Composting | 58 | Humidity=55% | CO2 produced | 130 | >90 | M.P. Balaguer et al., 2016 |
| PLA + Nano-CaCO₃ | Composting | 58 | Humidity=55% | Weight loss | 84 | 40.8 | M.P. Balaguer et al., 2016 |
| PLA + Nano-CaCO₃ | Composting | 58 | Humidity=55% | CO2 produced | 130 | >90 | M.P. Balaguer et al., 2016 |
| PLA + Nano-SiO₂ | Composting | 58 | Humidity=55% | Weight loss | 84 | 43.8 | M.P. Balaguer et al., 2016 |
| PLA + Nano-SiO₂ | Composting | 58 | Humidity=55% | CO2 produced | 130 | >80 | M.P. Balaguer et al., 2016 |
| PLA | Composting | 58 |  | CO2 produced | 75 | 100 | T. Narancic et al., 2018 |
| PLA/PCL (80/20) | Composting | 58 |  | CO2 produced | 75 | 100 | T. Narancic et al., 2018 |
| PLA/PBS (80/20) | Composting | 58 |  | CO2 produced | 75 | 100 | T. Narancic et al., 2018 |
| PLA/PHB (80/20) | Composting | 58 |  | CO2 produced | 75 | 98 | T. Narancic et al., 2018 |
| PLA | Soil |  | Humidity=30% | Weight loss | 98 | 12 | Wu, 2012 |
| PLA/Sisal (80/20) | Soil |  | Humidity=30% | Weight loss | 98 | 47~49 | Wu, 2012 |
| PLA/Sisal (60/40) | Soil |  | Humidity=30% | Weight loss | 98 | 67~70 | Wu, 2012 |
| PLA/NPK fertilizer (62.5/37.5) | Soil | 30 | Humidity=80% | Weight loss | 56 | 35-40 | Harmaen et al., 2015 |
| PLA/NPK fertilizer/EFB fiber (37.5/37.5/30) | Soil | 30 | Humidity=80% | Weight loss | 56 | 45 | Harmaen et al., 2015 |
| PLA | Soil | 25 | Humidity=35~40% | Decrease in soil TC | 28 | 13.8 | D. Adhikari et al., 2016 |
| PLA | Fresh Water | 30 | pH=7, sludge | O2 consumed | 28 | 3.7 | V. Massardier-Nageotte et al., 2006 |
| PLA | Fresh Water | 25 | 16h light and 8h dark | Weight loss | 365 | <2 | A.R.Bagheri et al., 2017 |
| PLA | Sea Water | 25 | 16h light and 8h dark | Weight loss | 365 | <2 | A.R.Bagheri et al., 2017 |
| PLGA | Fresh Water | 25 | 16h light and 8h dark | Weight loss | 270 | 100 | A.R.Bagheri et al., 2017 |
| PLGA | Sea Water | 25 | 16h light and 8h dark | Weight loss | 270 | 100 | A.R.Bagheri et al., 2017 |
| PLA | Anaerobic | 55 | pH=8.5, sludge | Conversion to biogas | 60 | 90 | H. Yagi et al., 2009 |
| PLA | Anaerobic | 37 | Sludge | Conversion to biogas | 277 | 49 | H. Yagi et al., 2009 |
| PLA | Anaerobic | 37 | Sludge | Conversion to biogas | 277 | 29 | H. Yagi et al., 2009 |
| PLA | Anaerobic | 55 | pH=8.0~8.3 | Conversion to biogas | 75 | 75 | H. Yagi et al., 2009 |
| PLA | Anaerobic | 55 | pH=8.0 | Conversion to biogas | 80 | 83 | H. Yagi et al., 2009 |
| PLA | Anaerobic | 52 |  | Conversion to biogas | 80 | 88 | T. Narancic et al., 2018 |
| PLA/PCL (80/20) | Anaerobic | 52 |  | Conversion to biogas | 121 | 90 | T. Narancic et al., 2018 |
| PLA/PBS (80/20) | Anaerobic | 52 |  | Conversion to biogas | 121 | 85 | T. Narancic et al., 2018 |
| PLA/PHB (80/20) | Anaerobic | 52 |  | Conversion to biogas | 80 | 100 | T. Narancic et al., 2018 |

2. PHA-based bioplastics

| Bioplastic | Environment | Condition |  | Indicator | Period (day) | Biodegradability (%) | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Temp.(℃) | Etc |  |  |  |  |
| PHB | Composting | 55 |  | CO2 produced | 28 | 78~80 | R.Y. Tabasi, A. Ajji., 2015 |
| PHB/PBAT (50/50) | Composting | 55 |  | CO2 produced | 28 | 47~48 | R.Y. Tabasi, A. Ajji., 2015 |
| PHB | Composting | 58 |  | CO2 produced | 110 | 90 | Y.-X. Weng et al., 2011 |
| PHB | Composting | 58 |  | CO2 produced | 45 | 100 | T. Narancic et al., 2018 |
| PHB/PCL (60/40) | Composting | 58 |  | CO2 produced | 46 | 100 | T. Narancic et al., 2018 |
| PHB/PBS (50/50) | Composting | 58 |  | CO2 produced | 88 | 100 | T. Narancic et al., 2018 |
| PHB | Soil |  |  | Weight loss | 180 | 64.3 | Jain and Tiwari, 2015 |
| PHB/CAB (50/50) | Soil |  |  | Weight loss | 180 | 31.5 | Jain and Tiwari, 2015 |
| PHB (film) | Soil | 26~31 | Humidity=70~82% | Weight loss | 303 | 98 | Boyandin et al., 2013 |
| PHB (pellet) | Soil | 26~31 | Humidity=70~82% | Weight loss | 303 | 55 | Boyandin et al., 2013 |
| PHBV (film) | Soil | 26~31 | Humidity=70~82% | Weight loss | 303 | 61 | Boyandin et al., 2013 |
| PHBV (pellet) | Soil | 26~31 | Humidity=70~82% | Weight loss | 303 | 35 | Boyandin et al., 2013 |
| PHB (film) | Soil | 27~30 | Humidity=78~84% | Weight loss | 385 | 47 | Boyandin et al., 2013 |
| PHB (pellet) | Soil | 27~30 | Humidity=78~84% | Weight loss | 385 | 28 | Boyandin et al., 2013 |
| PHBV (film) | Soil | 27~30 | Humidity=78~84% | Weight loss | 385 | 14 | Boyandin et al., 2013 |
| PHBV (pellet) | Soil | 27~30 | Humidity=78~84% | Weight loss | 385 | 8 | Boyandin et al., 2013 |
| PHA | Soil |  | Humidity=35% | Weight loss | 60 | 35 | Wu, 2014 |
| PHA/Rice husk (60/40) | Soil |  | Humidity=35% | Weight loss | 60 | 90 | Wu, 2014 |
| PHA | Soil | 20 | Humidity=50% | CO2 produced | 660 | 69.2 | E.F. Gomez, F.C. Michel Jr., 2013 |
| PHB | Soil | 25 | pH=6.5, water content=16% | Weight loss | 9 | 40 | CA Woolnough et al., 2008 |
| P(HB-co-8HV) | Soil | 25 | pH=6.5, water content=16% | Weight loss | 9 | 50 | CA Woolnough et al., 2008 |
| PHB | Soil | 25 | pH=6.5, water content=16% | Weight loss | 9 | 18 | CA Woolnough et al., 2008 |
| P(HB-co-8HV) | Soil | 25 | pH=6.5, water content=16% | Weight loss | 9 | 10 | CA Woolnough et al., 2008 |
| PHBV (HV 12 mol%) | Soil | 25 | Relative humidity = 65% | CO2 produced | 180 | 75 | M.V. Acros-Hernandez et al., 2012 |
| PHBV (HV 43 mol%) | Soil | 25 | Relative humidity = 65% | CO2 produced | 180 | 70 | M.V. Acros-Hernandez et al., 2012 |
| PHBV (HV 47 mol%) | Soil | 25 | Relative humidity = 65% | CO2 produced | 180 | 59 | M.V. Acros-Hernandez et al., 2012 |
| PHBV (HV 52 mol%) | Soil | 25 | Relative humidity = 65% | CO2 produced | 180 | 74 | M.V. Acros-Hernandez et al., 2012 |
| PHBV (HV 64 mol%) | Soil | 25 | Relative humidity = 65% | CO2 produced | 180 | 60 | M.V. Acros-Hernandez et al., 2012 |
| PHBV (HV 72 mol%) | Soil | 25 | Relative humidity = 65% | CO2 produced | 180 | 62 | M.V. Acros-Hernandez et al., 2012 |
| PHB | Soil | 25 |  | CO2 produced | 136 | 100 | T. Narancic et al., 2018 |
| PHB/PCL (60/40) | Soil | 25 |  | CO2 produced | 256 | 100 | T. Narancic et al., 2018 |
| PHB | Sea Water | 21 |  | O2 consumed | 100 | 80 | Thellen et al., 2008 |
| PHB | Sea Water | 12~22 | Nature, pH=7.9~8.1 | Weight loss | 90 | 30 | Thellen et al., 2008 |
| PHBV (HV 12wt%) | Sea Water | 21 |  | O2 consumed | 70 | 90 | Thellen et al., 2008 |
| PHBV (HV 12wt%) | Sea Water | 12~22 | Nature, pH=7.9~8.1 | Weight loss | 90 | 33 | Thellen et al., 2008 |
| PHB | River Water | 32 | pH=7, Nature (on the sediment) | Weight loss | 56 | 70 | N. Sridewi et al., 2006 |
| PHB | River Water | 32 | pH=7, Nature (buried) | Weight loss | 56 | >90 | N. Sridewi et al., 2006 |
| PHB | Fresh water | 25 | 16h light and 8h dark | Weight loss | 365 | 8.5 | A.R.Bagheri et al., 2017 |
| PHB | Sea Water | 25 | 16h light and 8h dark | Weight loss | 365 | 8.5 | A.R.Bagheri et al., 2017 |
| PHB | River Water |  | Nature, in 1999 | Weight loss | 42 | 43.5 | T.G. Volova et al., 2007 |
| PHB | River Water |  | Nature, in 2000 | Weight loss | 31 | 34.6 | T.G. Volova et al., 2007 |
| 3-PHB (film) | Sea Water | 28.75 | Nature, pH=7~7.5 | Weight loss | 160 | 42 | T.G. Volova et al., 2010 |
| 3-PHB/PHV (film) | Sea Water | 28.75 | Nature, pH=7~7.5 | Weight loss | 160 | 46 | T.G. Volova et al., 2010 |
| 3-PHB (pellet) | Sea Water | 28.75 | Nature, pH=7~7.5 | Weight loss | 160 | 38 | T.G. Volova et al., 2010 |
| 3-PHB/PHV (pellet) | Sea Water | 28.75 | Nature, pH=7~7.5 | Weight loss | 160 | 13 | T.G. Volova et al., 2010 |
| PHB | Fresh water | 21 |  | CO2 produced | 56 | 90 | T. Narancic et al., 2018 |
| PHB | Sea Water | 30 |  | CO2 produced | 43 | 90 | T. Narancic et al., 2018 |
| PHB/PCL (60/40) | Sea Water | 30 |  | CO2 produced | 56 | 86 | T. Narancic et al., 2018 |
| PHB | Anaerobic | 37 | Sludge | Conversion to biogas | 26 | 93 | H.Yagi et al., 2014 |
| PHB | Anaerobic | 37 | Sludge | Conversion to biogas | 26 | 92 | H.Yagi et al., 2014 |
| PHB (pretreated) | Anaerobic | 35 | Sludge | Conversion to biogas | 40 | 91 | Benn and Zitomer, 2018 |
| PHB | Anaerobic | 35 | Sludge | Conversion to biogas | 40 | 67 | Benn and Zitomer, 2018 |
| PHB | Anaerobic | 55 | pH=8.0~8.3 | Conversion to biogas | 14 | 90 | H. Yagi et al., 2013 |
| PHB | Anaerobic | 37 | pH=7.2 | Conversion to biogas | 9 | 100 | D.-M. Abou-Zeid et al., (2001) |
| PHB | Anaerobic | 37 | pH=7.2 | Weight loss | 9 | 100 | D.-M. Abou-Zeid et al., (2001) |
| PHBV (11.6mol%) | Anaerobic | 37 | pH=7.2 | Conversion to biogas | 42 | 30 | D.-M. Abou-Zeid et al., (2001) |
| PHBV (11.6mol%) | Anaerobic | 37 | pH=7.2 | Weight loss | 42 | 60 | D.-M. Abou-Zeid et al., (2001) |
| PHB | Anaerobic | 52 |  | Conversion to biogas | 127 | 92 | T. Narancic et al., 2018 |
| PHB/PCL (60/40) | Anaerobic | 52 |  | Conversion to biogas | 80 | 100 | T. Narancic et al., 2018 |
| PHB/PBS (50/50) | Anaerobic | 52 |  | Conversion to biogas | 121 | 80 | T. Narancic et al., 2018 |

3. Starch-based bioplastics

| Bioplastic | Environment | Condition |  | Indicator | Period (day) | Biodegradability (%) | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Temp.(℃) | etc |  |  |  |  |
| Plastarch | Composting | 55 | Humidity=60% | CO2 produced | 85 | 50 | E.F. Gómez, F.C. Michel Jr., 2013 |
| Mater-Bi | Composting | 25 |  | Weight loss | 90 | 43 | C. Accinelli et al., 2012 |
| Mater-Bi | Composting | 30 | Humidity=55% | Weight loss | 72 | 26.9 | R. Mohee et al., 2008 |
| Cassava starch/glycerol (3/1) | Composting | Room Temp. | Aspergillus niger isolate | Weight loss | 10 | 29.89 | R.C. Nissa et al., 2018 |
| Plastarch | Soil | 20 | Humidity=50% | CO2 produced | 660 | 31.3 | E.F. Gomez, F.C. Michel Jr. |
| Mater-Bi | Soil | 25 |  | Weight loss | 90 | 37 | C. Accinelli et al., 2012 |
| Mater-Bi | Soil |  | Nature | Weight loss | 90 | 3.4 | C. Accinelli et al., 2012 |
| Starch/PBS (50/50, film) | Soil | 25 | Humidity=35~40% | Weight loss | 28 | 7.2 | D. Adhikari et al., 2016 |
| Starch/PBS (50/50, powder) | Soil | 25 | Humidity=35~40% | Decrease in soil TC | 28 | 24.4 | D. Adhikari et al., 2016 |
| Cassava starch/glycerol (3/1) | Soil | Room Temp. | Aspergillus niger isolate | Weight loss | 10 | 29.89 | R.C. Nissa et al., 2018 |
| Mater-bi | Fresh water | 30 | pH=7 | O2 consumed | 28 | 42.8 | V. Massardier-Nageotte et al., 2006 |
| Mater-bi | Sea water | Room Temp. | Seawater+sediments | O2 consumed | 236 | 68.9 | Tosin et al., 2012 |
| Mater-bi | Fresh water | 25 |  | Weight loss | 90 | 1.6 | C. Accinelli et al., 2012 |
| Mater-bi | Fresh water |  | Nature (littoral marsh) | Weight loss | 90 | 1.5 | C. Accinelli et al., 2012 |
| Mater-bi | Sea water | 25 |  | Weight loss | 90 | 1.7 | C. Accinelli et al., 2012 |
| Mater-bi | Sea water |  | Nature | Weight loss | 90 | 4.5 | C. Accinelli et al., 2012 |
| Cassava starch/glycerol (3/1) | Fresh water | 30 | Aspergillus niger isolate | Weight loss | 10 | 20.18 | R.C. Nissa et al., 2018 |
| Cassava starch/glycerol (3/1) | Fresh water | 30 | Aspergillus niger isolate | Weight loss | 10 | 11.46 | R.C. Nissa et al., 2018 |
| Mater-bi | Anaerobic | 35 | pH=7, sludge | Conversion to biogas | 28 | 23 | Massardier-Nageotte et al., 2006 |
| Mater-bi | Anaerobic | 35 | Liquid digestate | Weight loss | 30 | 24.1 | P.S. Calabro et al., 2020 |
| Mater-bi | Anaerobic | 55 | Liquid digestate | Weight loss | 30 | 37 | P.S. Calabro et al., 2020 |
| Mater-bi (pretreated) | Anaerobic | 35 | Liquid digestate, | Weight loss | 15 | 78.2 | P.S. Calabro et al., 2020 |
| Plastarch | Anaerobic | 37 | Sludge | Conversion to biogas | 50 | 26.4 | Gómez and Michel, 2013 |

4. Petroleum-based bioplastics

| Bioplastic | Environment | Condition |  | Indicator | Period (day) | Biodegradability (%) | Reference |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Temp.(℃) | Etc |  |  |  |  |
| PBAT | Composting | 55 |  | CO2 produced | 28 | 34~35 | R.Y. Tabasi, A. Ajji., 2015 |
| PBS | Composting | 58 | pH=7.5, humidity=50~55% | CO2 produced | 160 | 90 | A. Anstey et al., 2014 |
| PBS/soy meal (75/25) | Composting | 58 | pH=7.5, humidity=50~55% | CO2 produced | 140 | 90 | A. Anstey et al., 2014 |
| PBS/canola meal (75/25) | Composting | 58 | pH=7.5, humidity=50~55% | CO2 produced | 160 | 90 | A. Anstey et al., 2014 |
| PBS/corn gluten meal (75/25) | Composting | 58 | pH=7.5, humidity=50~55% | CO2 produced | 160 | 90 | A. Anstey et al., 2014 |
| PBS/switch grass (75/25) | Composting | 58 | pH=7.5, humidity=50~55% | CO2 produced | 170 | 90 | A. Anstey et al., 2014 |
| PCL | Composting | 50 | pH=7~8.5 | CO2 produced | 6 | 38 | K. Nakasaki et al., 2006 |
| PCL | Composting | 58 |  | CO2 produced | 45 | 100 | T. Narancic et al., 2018 |
| PBS | Composting | 58 |  | CO2 produced | 207 | 92 | T. Narancic et al., 2018 |
| PCL/starch/additives (75/16/9) | Soil | 20 | Humidity=40% | Weight loss | 540 | 39 | Di Franco et al., 2004 |
| PBS (film) | Soil | 25 | Humidity=35~40% | Weight loss | 28 | 1.2 | D. Adhikari et al., 2016 |
| PBS (powder) | Soil | 25 | Humidity=35~40% | Decrease in soil TC | 28 | 16.8 | D. Adhikari et al., 2016 |
| PVC | Soil | 28 | Soil only | Weight loss | 120 | 1 | A. Campos et al, 2012 |
| PVC | Soil | 28 | Soil + leachate | Weight loss | 120 | 1.3 | A. Campos et al, 2012 |
| PCL | Soil | 28 | Soil only | Weight loss | 60 | 89.7 | A. Campos et al, 2012 |
| PCL | Soil | 28 | Soil + leachate | Weight loss | 60 | 22 | A. Campos et al, 2012 |
| PVC/PCL (1/1) | Soil | 28 | Soil only | Weight loss | 120 | 1.9 | A. Campos et al, 2012 |
| PVC/PCL (1/1) | Soil | 28 | Soil + leachate | Weight loss | 120 | 1.6 | A. Campos et al, 2012 |
| PCL | Soil |  | Humidity=20% | Weight loss | 70 | <5 | C.-S. Wu, 2005 |
| PCL/chitosan (90/10) | Soil |  | Humidity=20% | Weight loss | 70 | 10 | C.-S. Wu, 2005 |
| PCL/chitosan (80/20) | Soil |  | Humidity=20% | Weight loss | 70 | 20 | C.-S. Wu, 2005 |
| PCL-g-AA | Soil |  | Humidity=20% | Weight loss | 70 | <5 | C.-S. Wu, 2005 |
| PCL-g-AA/chitosan (90/10) | Soil |  | Humidity=20% | Weight loss | 70 | <10 | C.-S. Wu, 2005 |
| PCL-g-AA/chitosan (80/20) | Soil |  | Humidity=20% | Weight loss | 70 | 15 | C.-S. Wu, 2005 |
| Nylon-4 | Soil | 25 | pH=7.5~7.6, humidity = 80% | Weight loss | 120 | 100 | K. Hashimoto et al, 2002 |
| PCL | Soil | 25 |  | CO2 produced | 136 | 92 | T. Narancic et al., 2018 |
| PCL | Fresh Water | 30 | pH=7, sludge | O2 consumed | 28 | 34.8 | V. Massardier-Nageotte et al., 2006 |
| PCL | Fresh Water | 30 | pH=7, sludge | O2 consumed | 28 | 37.7 | V. Massardier-Nageotte et al., 2006 |
| PBAT | Fresh Water | 30 | pH=7, sludge | O2 consumed | 28 | 15.1 | V. Massardier-Nageotte et al., 2006 |
| PBS | Fresh Water | 25 | Sludge | O2 consumed | 44 | 88 | H.S. Cho et al., 2011 |
| PCL/starch/aliphatic polyesters (55/30/15) | Fresh Water | 25 | Sludge | O2 consumed | 80 | 31 | H.S. Cho et al., 2011 |
| Nylon-4 | Sea Water | 25 | pH=8 | O2 consumed | 25 | 80 | K. Tachibana et al., 2013 |
| Nylon-4 | Fresh Water | 25 | pH=6.9, sludge | CO2 produced | 28 | 49 | K. Hashimoto et al., 2002 |
| PCL | Fresh Water | 25 | 16h light and 8h dark | Weight loss | 365 | <2 | A.R.Bagheri et al., 2017 |
| PCL | Sea Water | 25 | 16h light and 8h dark | Weight loss | 365 | <2 | A.R.Bagheri et al., 2017 |
| PCL | Sea Water | 30 |  | CO2 produced | 56 | 80 | T. Narancic et al., 2018 |
| PCL | Anaerobic | 37 | Sludge | Conversion to biogas | 277 | 22 | H.Yagi et al., 2014 |
| PCL | Anaerobic | 37 | Sludge | Conversion to biogas | 277 | 3 | H.Yagi et al., 2014 |
| PBS | Anaerobic | 35 | Sludge | Conversion to biogas | 139 | 83 | H.S. Cho et al., 2011 |
| PCL/starch (55/35) | Anaerobic | 35 | Sludge | Conversion to biogas | 100 | 2 | H.S. Cho et al., 2011 |
| PCL | Anaerobic | 55 | pH=8.0~8.3 | Conversion to biogas | 50 | 80 | H. Yagi et al., 2013 |
| PCL | Anaerobic | 37 | pH=7.2 | Conversion to biogas | 42 | 30 | D.-M. Abou-Zeid et al., 2001 |
| PCL | Anaerobic | 37 | pH=7.2 | Weight loss | 70 | 8 | D.-M. Abou-Zeid et al., 2001 |
| PCL | Anaerobic | 52 |  | Conversion to biogas | 127 | 95 | T. Narancic et al., 2018 |