Fabrication of pH/redox dual-responsive mixed polyprodrug micelles for improving cancer chemotherapy

Ji Luo1, Shuguang Zhang1, Peiyao Zhu, Wenke Liu, Jiang Du*

Department of Thoracic Surgery, The First Affiliated Hospital of China Medical University, Shenyang 110001, China

1J.L. and S.Z. contribute equally to this work.

*Corresponding author:

Jiang Du: E-mail: jiangdu@cmu.edu.cn

Figure S1 Chemical structures of polyprodrugs mPEG-b-PAE-cis-DOX (upper) and mPEG-b-PAE-ss-DOX (below).

Figure S2 Particle size (A) and PDI (B) of the MPPMs-1, MPPMs-2 and MPPMs-3 measured by DLS (n= 3, mean ± S.D.).

Figure S3 Particle sizes of the MPPMs-1 (A), MPPMs-2 (B) and MPPMs-3 (C) in PBS at pH 7.4 and 5 % glucose upon dilution at 1/10, 1/100 and 1/1000 of the original concentration of nanoparticles, which was 2 mg/mL (n = 3, mean ± S.D.).

Figure S4 The in vitro DOX release profiles of MPPMs-2 (left) and MPPMs-3 (right) in PBS at different conditions (pH 7.4, pH 6.5, pH 7.4 with 10 mM DTT and pH 6.5 with 10 mM DTT) (n = 3, mean ± S.D.).

Figure S5 The cytotoxicity of diblock copolymer mPEG-b-PAE against NIH 3T3 cells for 24 h in concentration specified.

Figure S6 The fluorescence intensity of free DOX and three MPPMs treated cells confirmed by ImgeJ software based on Figure 7.

Figure S7 The tumor inhibitory rate of free DOX and MPPMs-2 at 20-day.

Figure. S8 The weight of major organs of mice treated with PBS, free DOX, and MPPMs-2, respectively. P values: **p<0.01, N.S., no significant difference.

Figure. S9 Blood biochemistry analysis of the mice treated with PBS, free DOX, and MPPMs-2, respectively. The results show mean and standard deviation of total bilirubin (TBIL), aminotransferase (ALT), aminotransferase (AST), blood urea nitrogen (BUN), uric acid (UA), creatinine (CREA), creatine kinase (CK). P values: *p<0.05, **p<0.01.